## Slide 1
Pooja Sahu
psahu@barc.gov.in
Chemical Engineering Division
Bhabha Atomic Research Centre
Department of Atomic Energy
India
Molecular Dynamics Simulations of Sodium Borosilicate Glasses for
Nuclear Field Applications

## Slide 2
Glass in Nuclear Industries
Nuclear Waste management and glass vitrification
Microscopic glass structure
Network formers, network modifiers and intermediate oxides
Computational Protocols
Software, Interaction potential and simulation methodology
MD simulated glasses
Mono-oxide, binary and tertiary glass mixtures
Conclusion
Outline

## Slide 3
Glass in Nuclear Industries
Treatment and Conditioning of HLW
Treatment
Long term storage : converting into relatively insoluble, compact solids and then eventual deposit into a geological repository
Source
Spent fuel from commercial/research reactors,
Liquid waste from the reprocessing of spent fuel
Waste from the nuclear weapons and propulsions industry
Need of Computer simulations
Handling of Radioactive Materials
High Temperature Process
Long term activities: leaching, chemical reactivity and
mechanical disintegration
Understanding of the process

## Slide 4
Oxides of P-block elements : Si, B, P, Ge
Strong bonds to oxygen
Coordination is sharply defined
Network Modifier
Network Former
Oxides of S block elements : Na, Ca
Weak, non-directional bonds to oxygen
Flexible coordination geometries
Broad distribution over bond lengths, and coordination
Intermediates
Oxides of Al, Ti, V and Mo participate as network former in presence of other oxides
Depending on composition may act either as network former or as network modifier.
Microscopic Glass Structure
Notes: B4 going into details I would like to present a brief overview about basic structure of glass ..

## Slide 5
Computational Protocols
BKS Potential: (Parameterized by combining microscopic (ab initio computations) and macroscopic (experimental) data
This potential better-models the repulsive Interaction at modest nuclear distances
Melt: Heated @ 5000 K to remove associated memory effects
Quench: Quenched @ 0.4K/ps to create amorphous system.
Equilibration and Data Collection: equilibrate to room conditions and analyzed the data collected.
Interaction Potential

## Slide 6
Mono-oxide Glasses
SiO2 and B2O3
2.38 g/cm3
1.82 g/cm3
LO-Si-O = 109.47o
LO-B-O = 120o
Tetrahedral coordination of Si
three-fold coordination of B
FSDP at 1.2-1.3 Å-1 for SiO2 and 1.45-1.65 Å-1 for B2O3
first peak at ~2.15-2.25 Å-1 and second peak at around 5.45 Å-1 for SiO2, first peak at 2.4-2.45 Å-1 and negative dip at 3.0 Å-1 for B2O3
SiO2 show a flat peak at 200-600 cm-1 and another peak at high frequencies ~1050-1070 cm-1
B2O3, shows four characteristic peaks at 130 cm-1 , 670 cm-1 , 960 cm-1 and 1180 cm-1

## Slide 7
Binary-oxide Glasses
Borosilicate
Si
O
B
Increasing density and
enhanced network connectivity with increasing SiO2
LO-Si-O = 109.47o
LO-B-O = 120o
Tetrahedral coordination of Si
Three and four fold coordination of B

## Slide 8
Ternary Sodium-borosilicate (NBS) glass
2.42 g/cm3
[106Na2O.123B2O3.370SiO2]
Average CN of O atoms:
Si=4, B=3.8 and Na=10.28
RDF peak position:
Si=1.62, B=1.48 and Na= 2.55Å
Tg = 542oC
Maximum density and BO4 fraction at 40% Na2O

## Slide 9
Effect of Composition : NBS glass
Composition of NBS glasses |  |  |  |  | 
 | NSiO2 | NB2O3 | NNa2O | R (NNa2O/ NB2O3) | K (NSiO2/ NB2O3)
NBS1 | 55% | 20% | 25% | 1.25 | 2.75
NBS2 | 60% | 20% | 20% | 1 | 3
NBS3 | 53% | 27% | 20% | 0.75 | 2
 | Density [g.cm-3] | % NBO | % B4
NBS1 | 2.273(*2.42) | 19.77 | 58.44
NBS2 | 2.275(*2.43) | 16.23 | 57.26
NBS3 | 2.269(*2.38) | 17.57 | 48.42
Density  SiO2 content
NBO  Na2O and then SiO2
BO4  Na2O and then SiO2 content
SiO2
B2O3
Na

## Slide 10
Short Range Order : Bond/Angle distribution
Average Coordination Number |  |  | 
Pairs | NBS1 | NBS2 | NBS3
Si-O | 4.00 | 4.00 | 4.00
B-O | 3.67 | 3.63 | 3.56
Na-O | 5.67 | 6.00 | 5.54
Si-Si | 1.77 | 2.03 | 1.15
Si-B | 1.94 | 1.82 | 2.81
B-B | 1.22 | 1.23 | 1.47
Na as charge compensator have lower CN
No effect on SiO4 tetrahedrals
B-O CN as per BO4 content
X-X CN as per SiO2 and B2O3 content

## Slide 11
Medium Range Order : Structure Factor
Splitting of FSDP for NBS1 and NBS3
Overlapped peaks/dips for NBS1 and NBS2
The major differences are noticed in position and shape of the peaks/dips at lower k i.e. 1-10 Å-1, which are related with the medium range structure of the glass

## Slide 12
Medium Range Order : Network connectivity
Si-O-B4 favored over Si-O-Si
The intermixing of B3 and B4 i.e. B3-O-B4 connections preferred over either of B3-O-B3 or B4-O-B4 connections
On Contrary to ”B[4] avoidance” rule, the present study showed abundant presence of B4-O-B4 units
NBS1 & NBS2 : Si-O-B4 > Si-O-Si > Si-O-B3 > B3-O-B4 > B4-O-B4 > B3-O-B3
NBS3: Si-O-B4 > Si-O-B3 > Si-O-Si > B3-O-B4 > B4-O-B4 > B3-O-B3
Probability of connection between structural units |  |  |  |  |  | 
 | Si-O-Si | Si-O-B3 | Si-O-B4 | B3-O-B3 | B3-O-B4 | B4-O-B4
NBS1 | 20.73 | 8.87 | 34.41 | 0.89 | 4.875 | 4.30
NBS2 | 23.68 | 9.90 | 30.55 | 1.09 | 4.54 | 3.30
NBS3 | 12.49 | 16.97 | 39.79 | 2.21 | 7.55 | 4.85

## Slide 13
 | NBS1 | NBS2 | NBS3
Young Modulus (GPa) | 40.65 | 42.74 | 39.66
Intrinsic strength (GPa) | 2.5 | 3.25 | 3.4
Yield Strength (GPa) | 1.92 | 2.15 | 2.51
Mechanical Strength : Stress-strain analysis
Deformation achieved via opening of angles
Plastic like deformation prior to brittle fracture
Young Modulus  SiO2 content
Yield & Intrinsic strength  primary by B2O3 then secondary by Na2O content

## Slide 14
Chemical Durability : Diffusivity
Diffusivity of sodium ions (DNa) and boron atoms (DB) [unit ˣ10-7 cm2/sec] at 600K |  | 
Glass | DNa | DB
NBS1 | 0.374±0.012 | 0.359±0.016
NBS2 | 0.235±0.009 | 0.221±0.013
NBS3 | 0.190±0.011 | 0.182±0.007
D of Na higher than B
D maximum for NBS1(high Na2O) and minimum for NBS3 (lower SiO2)
Increasing D with temperature

## Slide 15
Thermal Stability
Glass Transition temperature Tg & Thermal Expansion Coefficient (TEC)
 | NBS1 | NBS2 | NBS3
Tg [0C] | 567.63 (*518) | 572.31 (*537) | 481.79 (*489)
TEC [x10-5] /0C | 1.13 (*1.05) | 0.73 (*0.88) | 1.05 (*0.89)
Highest SiO2 in NBS2 corresponded to maximum Tg
Highest B2O3 in NBS3 lead to lowest Tg
NBS1 showed the highest TEC due to the highest Na2O content
Lower SiO2 responsible for a higher TEC of NBS3 than NBS2

## Slide 16
Cs/Sr doped NBS glasses
Concentration 5% and 10% (by mass) of base NBS
Glass | Density(*exp) [g/cm3] | Tg (*exp) [K]
NBS | 2.42 (*2.4) | 590 (*560)
NBS-5Cs | 2.49 | 
NBS-10Cs | 2.56 (*2.5) | 545 (*532)
NBS-5Sr | 2.49 | 
NBS-10Sr | 2.55 (*2.6) | 540 (*526)
Order of diffusion: Si < O < B < dopant < Na
 | CN [Na-O] Rcut=3.75 Å | CN [Cs-O] Rcut=4.05 Å | CN [Sr-O] Rcut=4.05 Å
NBS | 10.28 |  | 
NBS-5Cs | 9.48 | 13.08 | 
NBS-10Cs | 8.47 | 12.82 | 
NBS-5Sr | 9.51 |  | 9.04
NBS-10Sr | 8.77 |  | 9.06
Effects similar as network modifiers
BO, related with charge and ionic radius (1.69Å for Cs+ and 1.33Å for Sr++) of dopants

## Slide 17
CONCLUSIONS
B-K-S potential model can be applied to study a wide range glass composition
The results well capture the boron anomalies for varied concentration of network formers and network modifiers
Results provide a microscopic understanding of the glass structure and phenomena associated with the change in the glass composition
The macroscopic observable properties can be explained from microscopic structure and dynamics of glasses
The present work will hence have great academic as well as technological significance for further guidance in the selection of suitable glass composition for vitrification.

## Slide 18
Future Objectives
Understanding the Leaching and Chemical Reactivity of glasses
Effect of Radiation damage in vitrified glasses
Effect of Doping glasses with various Actinides and other fission Products

## Slide 21
Kislay Bhatt and K. Vaibhav
BARC, India
Acknowledgement
Dr. Sk. Musharaf Ali
Head, LSS, BARC, India
K.T. Shenoy, Group Director, ChEG
S. Mukhopadhyay, Head, ChED
ANUPAM Super Computing Facility, BARC, India
Computational collaborators
Arvind, G. Sugilal, and C. P. Kaushik
BARC, India
UK-India Civil Nuclear Collaboration (EP/T016337/1)

## Slide 22
Thank You

## Slide 24
2.2.6 Glass transition temperature (Tg)
The glass transition temperature of the constructed glass matrix was determined from the plot of inverse density vs. temperature over a range of temperature corresponding from glass state to melt state. The data points of both the zones were fitted to straight line using least square method, and intersection point of the fitted lines to glass zone and melt zone were used to determine the glass transition temperature44.