Scaling of deformation-induced microstructures in fcc metals

Darcy Hughes

Center for Materials and Engineering Sciences

Sandia National Laboratories, Livermore, CA 94550 USA

Microstructures developing during warm and cold monotonic deformation of fcc metals and alloys are described and reviewed. Similarities in the microstructural pattern that develop are demonstrated by the use of scaling laws. This analysis shows that the microstructural pattern develops similarly with the same mix of dislocation mechanisms for a wide range of materials, stress, strain, stacking fault energy (SFE), temperature, strain rate and monotonic deformation mode. The one requirement is for the three-dimensional dislocation mobility to be sufficient for the creation of three dimensional boundary structures.

This work was supported by the Office of Basic Energy Sciences, the U.S. DOE under contract no. DE-AC04-94AL85000.