## Slide 1: Hybrid systems for enhanced CO2 conversion into energy products and chemicals
Michele Aresta
CIRCC, via Celso Ulpiani 27, 70126 Bari
michele.aresta@uniba.it
ChBE Department, NUS, Singapore
cheam@nus.edu.sg
NUS
Interuniversity
Consortium
CHEMICAL REACTIVITY and CATALYSIS
I S C M T R P
2
5
8
2
W O R K S H O P
Trieste, May 21st, 2014

## Slide 2: Where we are, what we do…..
Director:
Prof. A. Dibenedetto
R&D Manager:
Prof. M. Aresta
www.circc.uniba.it
19 Universities
73 Research Units
Over 350 permanent staff

## Slide 3: People working on Innovative Catalysis for Carbon Recycling
The Team in Bari
  Prof. Angela Dibenedetto Carbonates, Aquatic Biomass
  Prof. Eugenio Quaranta Carbamates, Depolymerization
  Carlo Pastore, PD Ligno-cellulosic materials
  Antonella Angelini, PD Heterogeneous catalysts s&c
  Cristina Roth, PD Innovative Syntheses
  Tomasz Baran, PhD CO2-reduction, Photocatalysis
  Luigi Di Bitonto, PD Synthesis of cyclic carbonates
  Antonella Colucci, MSc Water-free trans-esterification of bio-oils
  - Guendalina Galluzzi,MSc Single pot Extraction/conversion of bio-oils
  Sheila Ortega, MSc Hybrid-polymers
  Stefania Fasciano, MSc Alcoholysis of urea
  Daniele Cornacchia Hydrogenation
  The NUS Group
  Prof. Sibudjin Kawi Reactive membranes, DRM
  The Krakow Group
  Prof. Wojciek Macyk Photocatalysis
EU FP7 IP,
ERANET CAPITA
EU FP6 IP TOPCOMBI, FP4 RUCADI Project
MiUR PRIN, FIRB, PON 2010, Technological Clusters
ENI, FCRP, TOTAL
€

## Slide 4: Agenda
The linear C-based economy
The role of CCU in CO2 emission reduction
CO2 conversion into energy products
Man-made photosynthesis: hybrid systems
From CO2 to methanol
The “co-factor” issue
A photochemical approach to NAD+ reduction to NADH and the integrated system
Photocatalytic carboxylation of organics
Conclusions

## Slide 5: The linear C-economy
CO2-emission control technologies
Efficiency in the production and utilization of energy 
Fuel shift
Use of renewables (biomass: not ubiquitary and limited)
Use of perennial sources: SWGH
CO2 capture followed by
  Disposal-CCS cost, permanence, site specificity…
  Utilization-CCU  Technological, Enhanced Biological, Chemical
Fossil-C  Thermal Energy + CO2
Mechanical  Kinetic
Electric
Chemical
28<h<50

## Slide 6: Maximization of C-utilization
Carbon Utilization Fraction: CUF < 1
Cproducts/Craw materials
Carbon Footprint: CF  very high
Efactor: Waste/Product  very high
(up to > 100)
Energy Consumption Ratio: ECR>1
Ein/Eout

## Slide 7: CCU: benefits and challenges
Affords added value products from a waste
  Fine chemicals, bulk chemicals, materials, fuels
Reduces fossil fuels extraction and dependence on natural reserves of carbon
Reduces the CO2 net immission into the atmosphere
Makes use of perennial energy sources for CO2 valorisation, mimicking Nature
May contribute to develop a
CO2/H2O-economy

## Slide 8: Gibbs standard free-energy
O

## Slide 9: Sources of CO2 (Except Power stations)
Industrial Sector | MtCO2/y produced
Oil Refineries | 850-900
Ethene and other Petrochemical Processes | 155-300
LNG Sweetening | 25-30
Ethene oxide | 10-15
Ammonia | 160
Fermentation | >200
Iron and steel | ca. 900
Cement | > 1000
1040-1245
ca. 2260
3300-3500 Mt/y
CO2
Concentration
may
considerably
vary

## Slide 10
CO2 separation technologies 1
Solid phases: CaO, MgO  Ca(Mg)CO3

Liquid phases: MEA, HOCH2-CH2NH2
HOCH2CH2NHCOO- +H3NCH2CH2OH
Silylamines: (RO)3Si-CH2CH2NHCH2CH2NH2
+
(RO)3Si-CH2CH2NH2CH2CH2NHCOO-
NH
CH2 COO-
CH2
NH2+
R

## Slide 11
CO2 separation technologies 2
Membranes (cost, space saving)
Ionic liquids (safety, cost, large volumes)
Combined systems
Cryogenic (cost, emissions of electricity)

## Slide 12: Actual use of CO2: 172 + 28 Mt/y Perspective use of CO2 to Chemicals
Compound | Formula Coxstate | Market 2016 Mt/y | CO2 Use Mt/y | Market 2030 Mt/y | CO2 use Mt/y
Urea | (H2N)2CO +4 | 180 | 132 | 210 | 154
Carbonates linear | OC(OR)2 +4 | >2 | 0.5 | 10 | 5
Carbonates cyclic | +4 |  |  |  | 
Polycarbonates | -[OC(O)OOCH2CHR]-n +4 | 5 | 1 | 9-10 | 2-3
Carbamates | RHN-COOR +4 | >6 | 1 | 11 | ca. 4
Acrylates | CH2=CHCOOH +3 | 5 | 1.5 | 8 | 5
Formic acid | HCO2H +2 | 1 | 0.9 | >10 | >9
Inorganic carbonates | M2CO3 +4 M’CO3 | CaCO3 250 | 70 | 400 | 100
Methanol | CH3OH -2 | 60 | 10 | 80 | 28
Total |  |  | 207 |  | 332

## Slide 13: CO2
Syngas
Resins
Chemicals
MTBE
CH2O
CH3COOH
TAME
C2, C4, Cn, C-O
CO
HCOOH
CH2O
CH3OH
CH4
DME
Methyl-derivatives: -amines
-acrylates
-halides
MTO, MTP, FUEL Cells
Perennial Energy
Water or waste
organics as H-source
Molecular carbonates
Poly-carbonates
RNHCOOR
RNCO
Poly-urethans
RNH2
NH3
H2NCONH2
Carbamates
Polymers
New chemicals
ROH
ROC(O)OR
Fuels additives
Solvents
Pharmaceuticals
Polymers…..
RCH=CHCOOH
RCH=CH2
HCs

## Slide 14
Chemicals
Dark Chemistry
Fuels
Light Chemistry
Use of
Low-entropy C
and Visible Light

## Slide 15: Energetics of CO2 reduction
Process | Potential
CO2 + e− → CO2•− | E◦ = −1.90V (-2.10 V in anhydrous media)
CO2 + 2H+ + 2e− → CO + H2O | E◦ = −0.53V,
CO2 + 2H+ + 2e− → HCO2H | E◦ = −0.61V
CO2 + 6H+ + 6e− → CH3OH + H2O | E◦ = −0.38V
CO2 + 8H+ + 8e− → CH4 + 2H2O | E◦ = −0.24V
Multi-electron
Multi-photon

## Slide 16: Short term: Use of excess electric energy
Use of off-peak production of electric energy for CO2 conversion into chemicals or fuels
  Fossil-C or Wind or Solar as primary sources
Option for the efficient storage of electric energy (still an open issue: batteries have a low energy to V or mass ratio, like H2!)
Use of fuels for transport or production of electric energy

## Slide 17: Volume energy density
Batteries 0.33 > 2.8
Liquid fuels as electricity storage: easily portable,
high energy density, use of existing infrastructures

## Slide 18: Short to Medium term: use of PV
Production and Use of PV
20 (40)% η StE
70-80% EtH (14  32% η in StH)
80-90% HtF (11  29% η in StF)
Mature technologies, ready to use!
Large volume electrolyzers, long-living electrodes
Plants: 1.2-1.8 % η StB
Algae: 6-10 (PBR)% η StB

## Slide 19: Cost of PV-H2 (and CH3OH)
Cost in € of 1 kgH2
3H2 + CO2  CH3OH + H2O
Cost of CH3OH 0.3 €/kg vs 0.08 €/kg BAU
But, if we consider the «carbon tax» then the cost of methaol would be around 0.16 €/kg

## Slide 20: PV Utilization
H2 production or direct electro catalytic reduction of CO2 in water?
Technology | H2 from H2O electrolysis followed by the catalysed reaction with CO2 to CH3OH | Direct (photo)electro-chemical reduction of CO2 in water
Solar light conversion efficiency, % | ca. 20 Expected 40% | ca. 20
Electrolysis Efficiency | 70-80 | 60-70
PH2/MPa in the electrolyzer | 0.1 | Not applicable
PH2/MPa in the chemical conversion | 30-50 | Not applicable
Temperature for CO2 conversion | 423 K | r.t.
Products (selectivity) | CH3OH (80-100) | H2-CO (ca. 20) CH3OH CH2=CH2 (ca. 80)

## Slide 21: Long Term: Photochemical reduction of CO2

## Slide 22: Natural systems for CO2 reduction
Enzymes
Co-factors
ATP  ADP, AMP…; NADH  NAD+;
Fdred  Fdox;…
Oxidized co-factors need to be reduced back to the energy rich form
Solar energy as primary source and secondary enzymes or other systems

## Slide 23
Mimicking Nature

## Slide 24: CO2 reduction to methanol
Exploit the fast rate and selectivity of enzymes
Stabilization of enzymes
Reduction of oxidized co-factor

## Slide 25: Hybrid systems: enzymes plus electrons and H+
Enzymes as catalysts
Co-factor is oxidized in the reduction of CO2
Reduce the oxidized form of the co-factor:
  Chemical systems
  Enzymes, cells
  Photocatalysts that use the solar light

## Slide 29
New devices

## Slide 30
Hybrid reduction of CO2
Use of ZnS-A and Ru/ZnS as light harvesting system (Xe)
From 3NADH/CH3OH to
>100 CH3OH/NADH
M. Aresta et al, ChemSusChem, 2012
390 nm

## Slide 31: Use of solar light
Photocatalysts that are active in the visible part of the spectrum
Cheap
Resistant
Tunable
Modified TiO2

## Slide 32: Band-Gap Modification
Cu2O
D
Dox
CB
VB
+
hv
-
NAD+
NADH
CrF5(H2O)2- @TiO2
CB
VB
-
hv
+
Ared
D
Dox
NAD+
NADH
-
rutin @TiO2
CB
VB
-
hv
+
Rutin
D
Dox
NAD+
NADH
NAD+
NADH
Fex/Zn1-xS
3dFe
D
Dox
CB
VB
+
hv
-
Patent 2013

## Slide 34: The effect of coupling the photocatalysts to the mediator

## Slide 35
D
Dox
CB
VB
+
hv 
-
NAD+/NADH
-
RhIII/RhI
H+
RhIII-H
-
-
FateDH
FaldDH
ADH
CO2 + 3NADH
CH3OH + 3NAD+
Hybrid CO2 Reduction: Electron
cascade in the Vis-Light photochemical regeneration
of NADH using modified TiO2 as solar energy utilizer
and a Rh complex as e- and H - transfer mediator
From 3NADH/CH3OH to over 100-1 000 CH3OH/NADH!
M. Aresta, A. Dibenedetto, T. Baran, W. Macyk, Patent 2013

## Slide 36
Influence of the components on the production of
NADH from NAD+

## Slide 37: Device for the hybrid reduction of CO2
Two compartment A-B cell
A: the enzyme reduces CO2 to methanol and consumes NADH
B: NAD+ is converted back to NADH
Recycling of NADH

## Slide 38: Low alkanes valorization
C1-C4 streams from gas and oil processing
  CH4  CH3COOH
C-H activation
  Biological
  Chemical
  Photochemical
sp3 vs sp2

## Slide 39: Fate of the tail gas
Ethane extraction by turboexpansion and fractionation without mechanical refrigeration
Cracking  methane, ethane, ethene, propene, propane, butene, butane, and higher HCs
Separation (C1, C2, C2=, C3, C3=; C4, C4=, >C4)
Solvent absorption and hydrogenation

## Slide 40: Photochemical conversion of LAs
CatPhoto + hv  h+ + e- (1)
CH4 + h+  •CH3 + H+ (2)
CO2 + e-  •-CO2 (3)
•CH3 + •CH3  CH3-CH3 (4)
CH4 + •CO2-  CH3COO- + •H (5)
CH3COO- + H+  CH3-COOH (6)
•CO2- + •H  HCOO- (7)
HCOO- + H+  HCOOH (8)

## Slide 41: Carboxylation of activated C-H Comparison of chemical and photochemical paths
  CH3COCH2COCH3  CH3COCH(COOH)COCH3
    OH
    CH3COCH=CCH3
    R’R”IM=CO2 + Sub-H + MX  R’R”IMH+X- + SUB=CO2M
    Chiusoli, PhONa, 1960-70
    Aresta et al, 2003
    ZnS, hv
  CH3COCH2COCH3  CH3COCH(COOH)HCOCH3 +
CH3COCH2COCH2-COOH
Aresta et al., ChemPlusChem, 2014

## Slide 42: The mechanism?
    OH hv O.
    CH3COCH=CCH3  CH3COCH=CCH3 + H.
    CH3COCH2C=CH2
    . O O
    CH3COCH-CCH3 CH3COCH2-C-CH2.
    .
CH3COCH2COCH3  CH3COCHCOCH3
CH3COCH2COCH2.
O

## Slide 43: Work in progress
Photocatalysis Applied to Complex Molecules
Systems bearing sp3 and sp2 C, plus C-O bonds have been used
Interesting information about the order of reactivity of the various bonds
Influence of CO2 on photochemistry of systems

## Slide 44: SPC Thermal Reactions
CO2 reduction
  MOx  MOx-1 + 1/2O2
  MOx-1 + CO2  MOx + CO
Water splitting
  H2O  H2 + 1/2O2
Net reaction
  CO2 + H2O  CO + H2 + O2

## Slide 45
Direct carbonation of olefins.
Several issues….
C
C
O
C
O
Ph
H
H
H
O
“one oxygen” transfer to the olefin”
“two oxygen” transfer to the olefin”
RCH=CH2
O2 / CO2
O2
RHC CH2
O
RCHO
RCOOH
RCH2CHO
RHC(O)CH3
1. The oxidation products distribution is mediated by CO2
2. An aldehyde is formed that promotes the formation of the epoxide
3. The latter is converted into the carbonate
4. Is it possible to avoid the double bond cleavage?
Detailed study on solvent, pressure of O2 and CO2, co-catalysts

## Slide 46: Epoxidation and carboxylation of olefins
  hv
  MOx + CH3CH=CH2  MOx-1 + CH3CH-CH2O
    Aresta-Dibenedetto, CatTod 2005
    MOx-1 + 1/2O2  Mox
    RCH-CH2O + CO2  RCH-CH2OC(O)O
    Not only the choice of the metal is crucial but also how the oxide is prepared: propene total oxidation

## Slide 47
Feedstocks for the Future Chemicals and Energy
short range
2030
Chemistry
oil and gas dominate
biomass will grow
CO2 utilization
Energy
mix
middle range
2050
Chemistry
oil and gas
coal
biomass will grow
Energy
switch to perennial
will be important
CO2 utilization
long range
>2050
Chemistry
Oil and gas
Coal (no CO2 problems)
Biomass at max
Energy
Substantial switch to perennial, world will go electricity
Large volumes CO2 used

## Slide 48: Conclusions
M. Aresta, A. Dibenedetto, N He for The Catalyst Group, 2013

## Slide 49
Key objective:
To reduce the impact on Climate Change.
by reducing the immission of CO2 (or other species with high CCP) into the atmosphere and the amount of climate alterating species (CAS) that accumulate in the atmosphere.
Question: is it enough to use CO2 for reaching the above goal?.
  The use of CO2 is not per se a guarantee that its emission is reduced.
  The new process (conversion or technological use) or product (substitute of existing ones) must minimize the use of materials, the energy consumption and the emission of CO2
Thanks for your attention!
Apulia
V-IV Century b.C.
Still
a lot
to think
about, but… I see the light!

## Slide 50: From the basket of published Books…..
1986
1989
2003
2003
2009
M. Aresta et al,
Chemical Reviews 2014
Notes: 50