## Slide 1: Solar thermochemical CO2 and H2O splitting via metal oxide redox reactions
P. Furlera, J.R. Scheffea, D. Marxera, A. Steinfelda,b
a Dempartment of Mechanical and Process Engineering, ETH Zurich, Switzerland
b Solar Technology Laboratory, Paul Scherrer Institute, Switzerland

## Slide 2: Outline
Introduction
  Thermochemical fuel production
  2-step CeO2 cycle
  Solar reactor design
  Experimental setup
Syngas production by splitting of H2O and CO2
Reactive CeO2 structures
Solar fuel synthesis
Summary and conclusions
Perspectives

## Slide 3: Solar thermochemical fuel production
Heliostat array
Absorber
Solar concentration
Image: http://www.brightsourceenergy.com/
Qsolar
H2O/CO2dissociation
H2O/CO2
H2/CO
O2
Catalytic fuel synthesis
Liquid fuels
(Diesel, Jet fuel,
Ethanol…)
CO2 capture

## Slide 4
Solar H2O / CO2 splitting
2-Step CeO2 cycle
H2 / CO
2nd step: oxidation
O2
H2O/CO2
liquid
fuels
(diesel, jet fuel…)
recycle
CO2 capture
1st step : solar reduction
Ce
Journal of Physics and Chemistry of Solids, 1975, 36, 1213-1222.

## Slide 5: ETH Solar Reactor
Reactor Front (water-cooled)
Reactor
Porous CeO2
Al2O3-SiO2
insulation
Inconel Shell
Quartz Window
Inlet
Purge Gas (Ar)
Inlet
Outlet
Concentrated
Solar Radiation
1500 ° C
O2
O2
O2
900 ° C
H2O / CO2
CO
H2
H2
Thermal Reduction:
2. Oxidation
Science 2010, 330 (6012), 1797-1801
Energy Environ. Sci. 2012, 5 (3), 6098-6103
Energy Fuels 2012, 26 (11), 7051-7059
X 1000 100 μm
X 1000 100 μm
Syngas
(H2 / CO)
10 mm

## Slide 6: Experimental setup
Energy Environ. Sci. 2012, 5 (3), 6098-6103

## Slide 7: Syngas production by simultaneous splitting of CO2 and H2O

## Slide 8: Experimental results Simultaneous H2O / CO2 splitting (H2O:CO2 = 5.7)
Experimental conditions: | Reduction | Oxidation
Power input: | 3.6 kW | 0.8 kW
Gas flows: | Ar: 2 l min-1 | Ar: 2 l min-1 CO2: 0.375 l min-1 H2O: 2.15 l min-1
Ceria structure: | Ceria Felt Total Mass: 127 g | 
Stoichiometric fuel production as expected (O2:fuel = 1:2)
(H2O → H2 + 0.5 O2)
(CO2 → CO + 0.5 O2)
No gas phase hydrocarbons detected
No C depositions
Energy Environ. Sci. 2012, 5 (3), 6098-6103
No impurities detected which could damage catalyst of FT unit

## Slide 9: Experimental results Syngas composition (H2:CO) vs. co-feeding ratio (H2O:CO2)
Experimental conditions: | Reduction | Oxidation
Power input: | 3.6 kW | 0.8 kW
Gas flows: | Ar: 2 l min-1 | Ar: 2 l min-1 CO2: 0.29 - 1.39 l min-1 H2O: 1.11 - 2.21 l min-1
Ceria structure: | Ceria felt Total mass: 127 g | 
Syngas composition (H2:CO) adjustable
in a wide range (0.25-2.34) by controlling
the co-feeding ration (H2O:CO2)
Syngas composition increases linearly with increasing H2O:CO2 ratios
e.g. co-feeding with H2O:CO2 = 6.5 yields syngas with H2:CO = 2
Syngas suitable for FT synthesis
Energy Environ. Sci. 2012, 5 (3), 6098-6103

## Slide 10: Experimental results Consecutive H2O / CO2 splitting (H2O:CO2 = 6.7)
Experimental conditions: | Reduction | Oxidation
Power input: | 3.6 kW | 0.7 kW
Gas flows: | Ar: 2 l min-1 | Ar: 2 l min-1 CO2: 0.33 l min-1 H2O: 2.20 l min-1
Ceria structure: | Ceria Felt Total Mass: 127 g | 
Energy Environ. Sci. 2012, 5 (3), 6098-6103

## Slide 11
Solar-to-fuel energy conversion efficiency
ηsolar-to-fuel
0.15 %
Reactive Structure
Reactive Material
Heat and mass transfer properties
Doped CeO2
Other metal oxides
Perovskites
Reactor technology
Geometry and scale-up
Operating conditions
Heat recovery
Direct impact on fuel production cost
20 %

## Slide 12: Reactive CeO2 structures

## Slide 13: Structural improvements of Ceria
  Limitations:
  HT limited during reduction
  ╚►pores in mm-range
  ╚►vol. absorption → fast heating rates
  ╚► high specific mass → high mass loading
Science 2010, 330 (6012), 1797-1801
Energy Environ. Sci. 2012, 5 (3), 6098-6103
Energy Fuels 2012, 26 (11), 7051-7059
High SSA → rapid oxidation kinetics but low specific mass
HT limited during reduction step

## Slide 14: CeO2 Structure CeO2 RPC (Reticulated Porous Ceramic)
Macro-porous structure enables penetration and absorption of concentrated solar radiation
  Faster heating rates
  Temperature gradients minimized
  High mass loading within reactor (~1500 g)
Energy Fuels 2012, 26 (11), 7051-7059

## Slide 15: Comparison felt vs. RPC
Experimental Conditions | Reduction | Oxidation
Power Input: | 3.6 kW | 0.7 kW
Gas Flow: | 2 l min-1 Ar | 3 l min-1 CO2(g)
Ceria Structure: | Ceria RPC: 1416 g, Ceria felt; 90 g | 
Overall 17 times higher fuel production per cycle with RPC structure
x 1000 100 μm
x 1500 50 μm
CeO2 felt
CeO2 RPC
Energy Fuels 2012, 26 (11), 7051-7059
x 1000 100 μm
x 1500 50 μm

## Slide 16
Energy Fuels 2012, 26 (11), 7051-7059
Experimental results
Conditions | Reduction | Oxidation
Power Input: | 2.8 - 3.8 kW | 0 kW
Gas Flow: | 2 l min-1 Ar | 2 l min-1 CO2
Mass loading: | 1416 g | 

## Slide 17
Improved heat-transfer
Improved specific mass
η RPC = 1.7 %
=> 12x η Felt (0.15 %)
=> 4 x η bricks (0.4%)
Experimental results Solar-to-fuel conversion efficiency
Energy Fuels 2012, 26 (11), 7051-7059

## Slide 18: Structural improvements of Ceria
  Limitations:
  HT limited during reduction
  ╚►pores in mm-range
  ╚►vol. absorption → fast heating
Phys. Chem. Chem. Phys. 2014, 16 10503
Science 2010, 330 (6012), 1797-1801
Energy Environ. Sci. 2012, 5 (3), 6098-6103
Energy Fuels 2012, 26 (11), 7051-7059
High SSA → rapid oxidation kinetics but low specific mass
HT limited during reduction step
  2) SSA limited during oxidation
  ╚►pores in the µm-range
  ╚► increase SSA → fast oxidation

## Slide 19
SEM micrographs single-scale RPC vs. multi-scale RPC
250 µm
250 µm
250 µm
Phys. Chem. Chem. Phys. 2014, 16 10503

## Slide 20: Experimental Setup Thermo-gravimetric analysis
CO2 Mixture
CeO2 sample

## Slide 21: Results TGA - CO2 splitting cycles
Oxidation time decreased from 28min to 3min (to reach 90% re-oxidation)
Experimental conditions | Reduction | Oxidation
Gas concentration: | PO2: 1.8*10-4atm | PCO2: 0.385 atm
Nonstoichiometry δ: | δi = 0.033 | δf = 0.0033
Phys. Chem. Chem. Phys. 2014, 16 10503

## Slide 22: Results TGA - CO2 splitting cycles
Experimental conditions | Reduction | Oxidation
Temperature: | 1500 °C | 1000 °C
Gas concentration: | PO2: 1.8*10-4atm | PCO2: 0.385 atm
Nonstoichiometry δ | δi = 0.033 | δf = 0.0033
Phys. Chem. Chem. Phys. 2014, 16 10503

## Slide 23: Results SEM micrographs
Only closed pores
Transition zone
Interconnected pore-network
Phys. Chem. Chem. Phys. 2014, 16 10503

## Slide 24: Results Consecutive CO2 splitting
Experimental conditions: | Reduction | Oxidation
Temperature: | 1500 °C | 1000 °C
Gas concentration: | PO2: 1.8*10-4atm | PCO2: 0.385 atm
Nonstoichiometry δ | δi = 0.033 | δf = 0.0033
Slightly decreasing rates due to moderate grain growth =► SSA: 0.098 → 0.089 m2 g-1
Constant CO-yields
Phys. Chem. Chem. Phys. 2014, 16 10503

## Slide 25: Results Solar reactor experiment
Conditions | Reduction | Oxidation
Power Input: | 3.8 kW | 0 kW
Gas Flow: | 2 l min-1 Ar (single) 6 l min-1 Ar (dual) | 2 l min-1 CO2 (single) 6 l min-1 CO2 (dual)
Mass loading: | single: 1416 g, dual: 998 g | 
Energy Fuels 2012, 26 (11), 7051-7059
Phys. Chem. Chem. Phys. 2014, 16 10503

## Slide 26: Solar fuel synthesis

## Slide 27: EU FP7 Project – SOLAR-JET 1st solar kerosene from H2O/CO2 splitting
Compressor station
FT-unit
(Shell Amsterdam)
290 H2O/CO2 splitting cycles
  200 h operation
  750 L syngas
  33.7% H2, 19.2% CO, 30.5% CO2, 0.06% O2, 0.09% CH4, 16.5% Ar
  No catalyst poisons

## Slide 28: EU FP7 Project – SOLAR-JET 1st solar kerosene from H2O/CO2 splitting
40.6 g liquid products
48.1 g solid waxes
  Hydrocracking of waxes (3.5 g):
  17.1 wt% Naphta (boiling range 0-145°C)
  35.6 wt% Kerosene (145-300°C)
  17.1 wt% Gasoil (300-370°C)
  30.2 wt% heavier fractions (>370°C)
World’s first solar kerosene from H2O and CO2 splitting

## Slide 29: Summary and conclusions
Heat transfer limitation during thermal reduction:
  RPC structure with pores in the mm-range
    Volumetric absorption => fast / homogenous heating
    Higher specific mass => higher ceria mass loading
Syngas production by simultaneous splitting of H2O and CO2
  Syngas composition can be controlled by the H2O/CO2 co-feeding radio
  Syngas is suitable for FT-synthesis (composition, purity)
Surface limitation during oxidation:
  Dual-scale RPC with pores in the mm-range and µm-range
    Increased SSA => fast oxidation kinetics
RPC structure allowed to enhance:
  the fuel production per unit time
  ηsolar-to-fuel = 1.7 %
1st solar kerosene from H2O/CO2 splitting in a solar reactor

## Slide 30: Perspectives Ongoing work and next steps
  Material-scale:
    Fundamental understanding of reaction mechanisms during red. / oxid.
    Efficient screening techniques for determining appropriate dopants and materials with the aim:
      Increasing the reduction extend
      Lowering the reduction temperature
operation at lower temperatures
System-scale
CO2 / H2O
supply
Catalytic fuel production plant
Reactor-scale
Structure-scale
Material-scale

## Slide 31: Perspectives Ongoing work and next steps
  Structure-scale:
    Optimization of pore-sizes for max. Ƞsolar-to-fuel
    Application of multi-scale approach to other structures such as honeycombs
  Reactor-scale:
    Scale-up and testing on solar dish / solar tower
    Optimization of cavity-receiver for max. Ƞsolar-to-fuel
    Alternative operation modes such as isothermal and vacuum operation
    Implementation of heat recuperation strategies
  System-scale:
    Integration and coupling of the individual components
    Assessment of operation modes (24/7 vs. day time operation)
    Economical simulation of the plant to assess production coast and guide development

## Slide 32: Acknowledgments
PREC ETH & STL PSI
EMPA: Dr. Ulrich Vogt,
Michal Gorbar, Alexander Bonk
Students: Louis Moes, Daniel
Marxer, Lukas Geissbühler,
Adrian Mularczyk
EU-SOLAR-JET
European Commission
Contract No. 285098
CCEM
EU-ERC Advanced Grant
SUNFUELS No. 320541