## Slide 1: Nano tools for macro problems: multiscale molecular modeling of nanostructured polymer systems
Maurizio Fermeglia
MOSE – DIA - University of Trieste Via valerio 10, 34127 Trieste (Italy)
Maurizio.Fermeglia@di3.units.it mose.units.it
Notes: Today, the discovery and optimization of new materials for innovative products is a time-consuming and laborious process, as much a craft practiced by skilled artisans as a science. Expensive trial-and-error-based experimentation is a highly inefficient way to screen potential candidates for a desired new application

## Slide 2: The technology vision 2020

## Slide 3: Nanoscale science and engineering
Ability to work at molecular level, atom by atom, to create large structures with fundamentally new properties and functions*
  At least one dimension is of the order of nanometers
  Functionality is critically dependent on nanoscale size
Promise of unprecedented understanding and control over basic building blocks and properties of natural and man-made objects*
Recent survey: Nanotechnology Long-term Impacts and Research Directions: 2010 – 2020 **
Theory, modeling and simulation (TMS)
  Expected to play key role in nanoscale science and technology
    INVESTIGATIVE TOOLS: THEORY, MODELING, AND SIMULATION, M. Lundstrom, P. Cummings, M. Alam, M. Ratner, W. Goddard, S. Glotzer, M. Stopa, B. Baird, R. Davis
    Springer, September 30, 2010
      Also available on the web at http://www.wtec.org/nano2/
* M. Roco, FY 2002 National Nanotechnology Investment Budget Request
** M.Roco, FY 2010 WTEC, Inc., 2010

## Slide 4: Horizon2020 Structure
KET

## Slide 5: Nanotechnology in different countries

## Slide 6: Materials Genome Initiative (MGI)
Developing a materials innovation infrastructure, through advances in and integration of:
  Computational tools
  Experimental tools
  Digital data and informatics
Achieving National goals in energy, security, and human welfare with advanced materials
Equipping the next generation materials workforce
Notes: Today, the discovery and optimization of new materials for innovative products is a time-consuming and laborious process, as much a craft practiced by skilled artisans as a science. Expensive trial-and-error-based experimentation is a highly inefficient way to screen potential candidates for a desired new application

## Slide 7: Materials Genome Initiative (MGI)

## Slide 8: Nanotechnology: global market evolution

## Slide 9: Molecular Simulation vs Theory
Advances in computational hardware and algorithms
  Moore’s law
    Gordon Bell Prize: 1Gflop/s in 1988 vs. 27 Tflop/s in 2002
    More than four order of magnitude increase in 14 years
    Add 2-3 orders of magnitude from parallelization (cheap today)
    Costs driven by consumer market
Notes: 9

## Slide 10: Moore’s law
Number of transistors on a sliver of silicon would double every two years

## Slide 11: Molecular Simulation vs Theory
Advances in computational hardware and algorithms
  Moore’s law
    Gordon Bell Prize: 1Gflop/s in 1988 vs. 27 Tflop/s in 2002
    More than four order of magnitude increase in 14 years
    Add 2-3 orders of magnitude from parallelization (cheap today)
    Costs driven by consumer market
Costs for experiment?
  Labor-intensive, high capital costs
Costs for theory?
  Labor-intensive 2
    Do graduate students and/or lab personnel/equipment improve by an order of magnitude every five years?
Notes: 11

## Slide 12: TMS: role of GPUs
Molecular complexity
  N. of time steps * n. atoms simulated in one day
Simple atom simulation
  For a simple monoatomic fluid is the n. of atoms that can be simulated for 10ns in one day

## Slide 13: New generation of products and productive processes (2000-2020)
Timeline for beginning of industrial prototyping and nanotechnology commercialization

## Slide 14: Multiscale Molecular Modeling
Notes: 14

## Slide 15: Multiscale Molecular Modeling
ACS Nano, 2012, 6(8): 7243-53
JACS, 133:20288-300 (2011)
Soft Matter, 2013, 9, 2936-2946.
J.Mat.Chem, 2012, 22, 5398-5409.
J.Mat.Chem, 20:7742-7753 (2010)
Mol. Simulation, 34: 1215-1236 (2008)
ACS App.Mat.Int., 2012, 4, 2855–2859
J.Multiscale. Mod., 3:151-176(2011)
Notes: 15

## Slide 16: Multiscale Molecular Modeling
J.Multiscale. Mod., 3:151-176(2011)
ACS Nano, 2012, 6(8): 7243-53
JACS, 133:20288-300 (2011)
Soft Matter, (2013) in press
J.Mat.Chem, 2012, 22, 5398-5409.
J.Mat.Chem, 20:7742-7753 (2010)
Mol. Simulation, 34: 1215-1236 (2008)
ACS App.Mat.Int., 2012, 4, 2855–2859
Notes: 16

## Slide 17: Modelling and experiments

## Slide 18: Outline of talk
Introduction
  Multiscale Molecular Modeling
Mapping procedure
  From atomistic simulation to mesoscale
  From mesoscale to micro FEM
Applications to nanostructured polymer systems
  Top down nanostructures
    Classical PCN
  Bottom up design
    Localization of gold nanoparticles in di-block copolymers
    Effect of chain length and grafting density
    Self assembly of nanostructures on gold nanoparticles
  Special applications
    Block copolymers for drug delivery
Conclusions
Notes: 18

## Slide 19: From atoms … to beads
Molecular Dynamics
Dissipative Particle Dynamics
ForceField based calculations
Soft potentials calculations
Fi = f (aii, aij, …, rc )
Polymeric materials are modeled by connecting beads by harmonic springs

## Slide 20: Parameters for mesoscale models
bead size and Gaussian chain architecture
  From characteristic ratio (C) in terms of Kuhn length
bead mobilities M,
  From bead self diffusion coefficients - MD
effective Flory-Huggins interactions
  Method 1: polymer blends, copolymers, spherical nanofillers
    Differences in non bonded energies between bulk and isolated chain
  Method 2: nanofillers of any size and shape
    From energy distribution in MD considering density distribution around nanofiller
Notes: Aggiungere il caso di non compatibilizzante

## Slide 21: bead size, chain architecture
MD NPT runs on homo polymers
  Monomer length
  C∞ calculation and Kuhn lenght
  Chain architecture
Rotational Isomeric State
C1
C2
C3
C4
Cn
MM minimization and annealing
MD - NPT
<r>2 – end to end distance
<r>2 / n l2 = C∞
Change chain lenght
C∞
Fermeglia, M. et al., Polymer, 47:5979-5989 (2006)

## Slide 22: Method 1: F-H interaction parameter chi
Molecular dynamics NPT and NVT runs
Fermeglia, M. and Pricl S., AIChE J., 2619 (45), 1999

## Slide 23: Estimation of DPD parameters from atomistic simulations
Single, binary, ternary energies from MD
Binding energies from MD
(vdW + Coulomb)
Define DPD beads
(head, tail, …) and
recalculate energies
Binding energies are
rescaled considering the
number of contacts
References DPD
Interactions are selected
Equal beads aij  25
Strong repulsive beads
aij  >25
DPD matrix parameters (scaling from references)
Density profiles from DPD
Density profiles from MD
=?
Scocchi et al., J. Phys. Chem. B, (2007), 111, 2143

## Slide 24: From beads to micro FEM
Dissipative Particle Dynamics
Soft potentials calculations
Fi = f (aii, aij, …, rc )
Characteristic dimension of mesoscopic system
Micro - FEM Simulation
FEM Analysis:
Macroscopic properties
Toth R., Santese F., Pereira S.P., Romero-Nieto D., Pricl S., Fermeglia M., Posocco, Journal of Materials Chemistry, 22, 5398-5409 (2012)

## Slide 25: From beads … to micro: fixed grid
Geometry: map cubes to Palmyra tetrahedrons
Laplace equation is solved for electric conductance, diffusion and permeability
Local deformation allow the calculation of mechanical properties
Fixed grid
Variable grid
Mesoscale
Atomistic
Physical Prop.
Pereira S.P, Scocchi G., Toth R., Posocco P., Romero-Nieto D., Pricl S., Fermeglia M., Journal of Multiscale Modeling, 3:151-176 (2012)

## Slide 26: microFEM modelling: variable grid
Platelets orientation
  Alignement is defined and assigned to each platelet
Pure component properties definition
  Properties of the stacks is based on mesoscale simulations
  Pure component properties from MD or experimental data
Pereira S.P, Scocchi G., Toth R., Posocco P., Romero-Nieto D., Pricl S., Fermeglia M., Journal of Multiscale Modeling, 3:151-176 (2012)

## Slide 27: Simulation protocol for core-shell nanoparticles
Atomistic interface
mesoscale interface
Density profile
of the interface
(DPD)
Mechanical properties
of the interface
(Mesosprop)
Mechanical properties
of the pure filler
Palmyra
filler
Volumetric average
of properties
Palmyra
simulation
Notes: DPD density profiles: sviluppato per sistemi senza compatibilizer, ma valido per sistemi grafted. Approccio è di calcolare le proprietà sulla zona di interfaccia e poi mappare il tutto in palmyra
Fatto con Accelrys MS, applicabile ai nostri sistemi se CULGI fornisce la conversione dei dati da coordinate in densità.

## Slide 28: Outline of talk
Introduction
  Multiscale Molecular Modeling
Mapping procedure
  From atomistic simulation to mesoscale
  From mesoscale to micro FEM
Applications to nanostructured polymer systems
  Top down nanostructures
    Classical PCN
  Bottom up design
    Localization of gold nanoparticles in di-block copolymers
    Effect of chain length and grafting density
    Self assembly of nanostructures on gold nanoparticles
  Special applications
    Block copolymers for drug delivery
Conclusions
Notes: 28

## Slide 29: Nano-structured materials

## Slide 30: Polymer clay nanocomposites
Molecular Dynamics (MD)
Dissipative Particle Dynamics (DPD)
~ 1 nm
~ 3 nm
~ 15 nm
~ 120 nm
Finite Elements Method (FEM)
~ 0.3 μm
1 nm
10 nm
100 nm
1 μm
~ 1 nm
100 - 500 nm
Notes: 30

## Slide 31: Summary of the results
  The chemical/physical characteristics of the different surface modifiers does not affect the macroscopic properties
  The size and shape of the filler and the properties of the pure nanocomposite components have a big impact on overall material properties.
Fermeglia et al., J. Mater. Chem. 2012, 22, 5398; Fermeglia et al., J. Multiscale Model. 2012, 3,1; Fermeglia et al., Chem. Eur. J. 2009,15,7586; Fermeglia et al., Macromolecules 2009, 42, 21, 8260; Fermeglia et al. J. Phys. Chem B 2007, 111, 2143

## Slide 32: Macro level: nylon6+MMT
Fornes, T.D., et al., Effect of organoclay structure on nylon 6 nanocomposite morphology and properties. Polymer, 2002. 43(22): p. 5915-5933.
 | EXPERIMENTAL (4.5%) | EXPERIMENTAL (7.1%) | CALCULATED (4.6%)
 | Ec/Em | Ec/Em | Ec/Em
PA6+C20A | 1.57 |  | 1.61
PA6+C30B | 1.62 | 1.72 | 1.57
PA6+M3C18 | 1.69 | - | 1.60
C20A
M3C18
Notes: Papers in fodelr references
Data 7.1 % from deliverable MH

## Slide 33: Hydrotalcite + FA + PP
 | EXPERIMENTAL (5%) | CALCULATED (4.6%)
 | Ec/Em | Ec/Em
PP + FA +HT | 1.11 | 1.12
 | Tabuani et al. (2011) | 
Experimental data from Tabuani et al., Macromol. Symp. 2011, 301, 114–127
Pereira S.P., Scocchi G., Toth R., Posocco P., Nieto D.R., Pricl S., Fermeglia M., Journal of multiscale modelling, 3,1-28 (2012)

## Slide 34: TPU+MMT: thermal conductivity
 | EXPERIMENTAL (5%) | CALCULATED (4.6%)
 | kc/km | kc/km
TPU+C30B | 1.18 | 1.14
Wai K. Ho, Joseph H. Koo, and Ofodike A. Ezekoye, “Thermoplastic Polyurethane Elastomer Nanocomposites: Morphology, Thermophysical, and Flammability Properties,” Journal of Nanomaterials, vol. 2010, Article ID 583234, 11 pages, 2010. doi:10.1155/2010/583234
Pereira S.P., Scocchi G., Toth R., Posocco P., Nieto D.R., Pricl S., Fermeglia M., Journal of multiscale modelling, 3,1-28 (2012)
Notes: Comparison for the lowest T
34

## Slide 35: Permeability: PP + C20A
 | EXPERIMENTAL (6 wt%) | CALCULATED (4.6 wt%)
 | Pc/Pm | Pc/Pm
PP+MMT | 0. 78 | 0.75
Osman, M. A., et al., Poly(propylene)-Layered Silicate Nanocomposites: Gas Permeation Properties and Clay Exfoliation. Macromolecular Chemistry and Physics, 2007. 208(1): p. 68-75.
Same basal spacing
6 wt% corresponds to 2 vf%
Pereira S.P., Scocchi G., Toth R., Posocco P., Nieto D.R., Pricl S., Fermeglia M., Journal of multiscale modelling, 3,1-28 (2012)
Notes: Permeability careful that the comaptibilizer is different …. Consider only the MMT calcualtion is doen with C20A (same basal spacing)

## Slide 36: Influence of the degree of exfoliation
PP+PPgMA+C20A
Scocchi G., 2009, Multiscale Simulation of Polymer-Clay Nanocomposites, phd Thesis, University of Trieste

## Slide 37: PA6 – M2(C18)2 – CEC90
Cation Exchange Capacity: 90 meq/100g
M2(C18)2
PA6
T.D Fornes et al., Polymer 42 (2002) 5915
Scocchi G., 2009, Multiscale Simulation of Polymer-Clay Nanocomposites, phd Thesis, University of Trieste
Notes: 37

## Slide 38: PP – M2(C18)2 – CEC90
M2(C18)2
PP
M. T. Ton-That et al., Polym Eng Sci 44 (2004) 1212
Cation Exchange Capacity: 90 meq/100g
Scocchi G., 2009, Multiscale Simulation of Polymer-Clay Nanocomposites, phd Thesis, University of Trieste
Notes: 38

## Slide 39: Dogbone ASTM D638 samples at a strain rate of 5 mm/min
2-PP+PPgMA+C20A nanocomposite
3-PP+Hydrotalcite nanocomposite

## Slide 40: Uniaxial compression at a constant strain rate (5 mm/min) of the demonstrators
Deformed shape and force/displacement curves for PP+PPgMA+C20A nanocomposite Bottle.
Deformed shape and force/displacement curves for PA6+C30B nanocomposite glass.

## Slide 41: Outline of talk
Introduction
  Multiscale Molecular Modeling
Mapping procedure
  From atomistic simulation to mesoscale
  From mesoscale to micro FEM
Applications to nanostructured polymer systems
  Top down nanostructures
    Classical PCN
  Bottom up design
    Localization of gold nanoparticles in di-block copolymers
    Effect of chain length and grafting density
    Self assembly of nanostructures on gold nanoparticles
  Special applications
    Block copolymers for drug delivery
Conclusions
Notes: 41

## Slide 42: Nano-structured materials

## Slide 43: Self assembly of nanoparticles in block copolymers
Organic polymer and inorganic particles mixing (PPNs)
  PPNs fabrication process via self-assembly
  By dispersion of particles in diblock copolymers
Predicted microstructure morphology depends on
  nature of the system
    chemistry and architecture of the blocks
    volume fraction of the nanoparticles
    strength and type of interactions
  process conditions
    temperature
    shear
SCOPE: model the system morphology
Experimental evidence by Chiu et al.
  poly styrene-2 vinyl pyridine
Applications:
  Opto electronic industry
Chiu, J.J, Bumjoon J.K., Kramer E.J. Pine, D.J., JACS, 2005, 127, 5036

## Slide 44: Lamellae: A (or B) covering
segregation in the center of the corresponding domain;
perfect agreement with experimental evidences.
Density
Distance
Maly M., Posocco P., Pricl S., Fermeglia M.. IEC, 47: 5023-5038 (2008)
Posocco P., Posel Z., Fermeglia M., Lísal M., Pricl S., J. Mater. Chem., 20:10511-10520 (2010)
Posel Z., Posocco P., Fermeglia M., Lisal M., Pricl S., Soft Matter, DOI: 10.1039/c2sm27360h (2013)
Notes: 44

## Slide 45: Lamellae: A and B covering (A6B6)
Density
Distance
nanoparticles at the interfaces between the A-B blocks
  Agreement with experiments
Notes: 45

## Slide 46: PS grafting only: loading: fp = 0.05
Migration to the interface (from a to d) for decreasing PS grafting density
  1D density profiles:
    a, PS4Au8;
    b, PS3Au9;
    c, PS2Au10,
    d, PS1Au11.
  Line legend:
    (green), PS;
    (blue),PVP;
    (red), Au.
Posocco P., Posel Z., Fermeglia M., Lísal M., Pricl S., J. Mater. Chem., 20:10511-10520 (2010)

## Slide 47: PS grafting only: loading: fp = 0.2
For PS4Au8 system, large regions of nanoparticles (red) – exp. evidence
Same tendency to migrate to the interface as the PS grafting density decreases
  Line legend:
    (green), PS;
    (blue),PVP;
    (red), Au.
Kim et al., Macromolecules, 39, 4198, 2006
PS4Au8
PS1Au11
Posocco P., Posel Z., Fermeglia M., Lísal M., Pricl S., J. Mater. Chem., 20:10511-10520 (2010)
Posel Z., Posocco P., Fermeglia M., Lisal M., Pricl S., Soft Matter, DOI: 10.1039/c2sm27360h (2013)

## Slide 48: Grafted silica nanoparticles in polymers
Particles embedded in a polymer matrix and grafted with polymer chains.
  Matrix: polydispersity, molecular weight
  Particles: size, chemical nature, surface treatment
  Grafting agents: chemical nature, grafting density, molecular weight, polydispersity
Grafted nanoparticles and semi crystalline polymers
  Core: amorphous SiO2 5-10 nm diameter
  Linker: Si based component
  Grafted polymer chains: polystyrene 2k – 20k
  Polymer: amorphous polystyrene 100k

## Slide 49: The model System
Grafted nanoparticles and semi crystalline polymers
  Core: amorphous SiO2 5-10 nm diameter
  Linker: Si based component
  Grafted polymer chains: polystyrene 2k – 20k
  Polymer: amorphous polystyrene 100k
Carved Sphere
Etched Sphere
Grafted Sphere
BrC(CH3)2CO2(CH2)3SiMe2Cl

## Slide 50: A general view of the project
Polystyrene – silica grafted nanoparticles: different scales:
Single nP MC
MD & Cg MD
DPD 1:1
DPD 1:n
DPD 1:many
Parameters from: COSMO-RS or MD
Increasing time and length

## Slide 51: Brush thickness: effect of grafted density
existence of a critical radius rDC
for h + r < rDC,  Concentrated Polymer Brush (CPB) regime
  dry brush - autophobic dewetting, particle aggregation;
for larger h +r  Semidilute Polymer Brush (SDPB) regime
  wet brush, good dispersion

## Slide 52: Aggregation vs. dispersion: effect of loading and grafting density
Fixed grafted chain length (20k) in PS 100k
Increasing grafted chains density leads to aggregation
Increasing nP concentration does not alter dispersion

## Slide 53: Comparison with experiments – CG level II
0.5% wt and 0.31 chains/nm2
0.5% wt and 0.82 chains/nm2
5.0% wt and 0.31 chains/nm2
5.0% wt and 0.82 chains/nm2
Grafting density
Concentration
dispersion/aggregation
dispersion
dispersion
aggregation

## Slide 54: Aggregation vs. dispersion: effect of grafted chain lenght
2.5k Da and 0.51 chains/nm2
103.7 k Da and 0.53 chains/nm2
21.3 k Da and 0.31 chains/nm2
Chain
length
aggregation
dispersion
dispersion
Increasing grafted chain length favors uniform distribution of nP in the matrix
Fixed grafted density and PS matrix 100k

## Slide 55: Comparison with experiments – CG level II
2k and 0.4 chains/nm2
100k and 0.53 chains/nm2
18k and 0.31 chains/nm2
18k and 0.82 chains/nm2
Chain
length
Grafting density
aggregation
dispersion/aggregation
dispersion
dispersion

## Slide 56: Lliterature

## Slide 57: Silica nP – Grafting density 0.5 chains/nm2 20kDa PS
% NP | EC (GPa) | EC/EM | h (nm)
1 | 2.59 (2.60) | 1.03 | 7.5
5 | 2.94 (2.82) | 1.17 | 9.3
10 | 3.45 | 1.37 | 10.2
1% v/v
5% v/v
10% v/v
Isolated Particles
Primary Aggregates
Long Strings

## Slide 58: Silica nP – Grafting density 0.7 chains/nm2 20kDa PS
1% v/v
5% v/v
10% v/v
% NP | EC (GPa) | EC/EM | h (nm)
1 | 2.62 | 1.04 | 10.7
5 | 3.07 | 1.22 | 10.3
10 | 3.55 | 1.41 | 11.0
Sheet Like
Isolated Particles
Primary Aggregates

## Slide 59: Silica nP – Grafting density 1.0 chains/nm2 20kDa PS
% NP | EC (GPa) | EC/EM
1 | 2.62 (2.75) | 1.04
5 | 3.34 (2.87) | 1.33
1% v/v
5% v/v
Isolated Particles
Long Strings

## Slide 60: Summary of the mechanical properties
% NP | EC (GPa) | EC/EM
Grafting density 0.5 chains/nm2 |  | 
1 | 2.59 | 1.03
5 | 2.94 | 1.17
10 | 3.45 | 1.37
Grafting density 0.7 chains/nm2 |  | 
1 | 2.62 | 1.04
5 | 3.07 | 1.22
10 | 3.55 | 1.41
Grafting density 1 chains/nm2 |  | 
1 | 2.62 | 1.04
5 | 3.34 | 1.33
LOW % NPs
ISOLATED NPs
EC/EM ≠ f(dg)

## Slide 61: Summary of the mechanical properties
% NP | EC (GPa) | EC/EM
Grafting density 0.5 chains/nm2 |  | 
1 | 2.59 | 1.03
5 | 2.94 | 1.17
10 | 3.45 | 1.37
Grafting density 0.7 chains/nm2 |  | 
1 | 2.62 | 1.04
5 | 3.07 | 1.22
10 | 3.55 | 1.41
Grafting density 1 chains/nm2 |  | 
1 | 2.62 | 1.04
5 | 3.34 | 1.33
INCREASING % NPs
DIFFERENT NPs MORPHOLOGIES
EC/EM = f(%NP)
Notes: Dati sperimetnali:
Grafting density

## Slide 62: Summary of the mechanical properties
% NP | EC (GPa) | EC/EM
Grafting density 0.5 chains/nm2 |  | 
1 | 2.59 (2.600.1) | 1.03
5 | 2.94 (2.810.2) | 1.17
10 | 3.45 | 1.37
Grafting density 0.7 chains/nm2 |  | 
1 | 2.62 | 1.04
5 | 3.07 | 1.22
10 | 3.55 | 1.41
Grafting density 1 chains/nm2 |  | 
1 | 2.62 (2.750.2) | 1.04
5 | 3.34 (2.870.1) | 1.33

## Slide 63: Self assembly of nanostructures on gold nanoparticoles
1
Color legend:
solvent=turquoise
TEG/PEG=green
C8=grey
F8=purple
gold=brown
Stripes
Stripe thickness ~ 0.65-0.7 nm
F8 ~ 1.2+ 3.1 nm
C8 ~ 1.3+ 1.9 nm
1
Posocco P, Gentilini C, Bidoggia S, Pace A, Franchi P, Lucarini M, Fermeglia M, Pricl S, Pasquato L., ACS Nano, 2012, 6(8):7243-53
Notes: Il grafico ti riporta una della rdf, quella per il florurato. Tieni presente che la rdf è fatta a partire dal CENTRO della nanoparticella. Per cui, ai valori, devi sottrarre il raggio della stessa (in questo caso, per sistema 1, è 1.1. nm). Come vedi, la curva viola è quella totale, e, prendendo il massimo del secondo picco, hai la dimensione più probabile della intera particella (core + shell) (raggio = 3.75 nm). Lo strato di florurato ha un’altezza più probabile di 1.2 nm, laddove la sua lunghezza fully stretched è 1.4 nm. Per il pezzo di peg attaccato, invece, come vedi una piccola parte si intrufola nel monolayer (primo picco verde puntinato a 1.1 nm), ma il grosso, come deve, sta fuori. La estensione dello strato di peg più probabile coincide con la parte viola, e quindi a 2.65nm, ma ci sono anche catene fully stretched (guarda la il modello della particella in alto a sinistra), che arrivano a 4.6 nm.

## Slide 64: Self assembly of nanostructures on gold nanoparticoles
2: effect of core size
Janus
nanoparticle
Stripe-like pattern
Color legend:
solvent=turquoise
TEG/PEG=green
C8=grey
F8=purple
gold=brown
3: effect of grafted composition
Domains
2: effect of core size

## Slide 65: Outline of talk
Introduction
  Multiscale Molecular Modeling
Mapping procedure
  From atomistic simulation to mesoscale
  From mesoscale to micro FEM
Applications to nanostructured polymer systems
  Top down nanostructures
    Classical PCN
  Bottom up design
    Localization of gold nanoparticles in di-block copolymers
    Effect of chain length and grafting density
    Self assembly of nanostructures on gold nanoparticles
  Special applications
    Block copolymers for drug delivery
Conclusions
Notes: 65

## Slide 66: Nanovectors in medicine
Typical properties:
  Biocompatibility
  Water solubility
  High specificity
  Multifunctionality
  Cell barriers crossing, ….
Liposomes → lipoplexes
Polymers → polyplexes
→ dendriplexes
Inorganic nanovectors (carbon nanotubes, fullerenes, …)
Viruses

## Slide 67: Objective: Di/triblock copolymers in water
Diblock copolymer PEG-PLA:
  Poly(ethylene oxide) PEG (Mw = 3670 Da)
  Poly-DL(lactic acid) PLA (Mw = 3300 Da)
Effect of copolymer composition and concentration on system morphology
Triblock copolymer PLA-PEG-PLA:
  PLA5875‐PEO7761‐PLA5875
Effect of polymer concentration on system morphology
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753
Notes: Caratteristiche di un sistema di rilascio di formci o RNSA- DNA : Solubilità, tossicità e rilascio controllato
Come ? Virus (solo epr RNA e DNA) oppure polineri. Noi facciamo polimeri con small molecules.
Polimero bio compatibili
Goals: digarammi di fase predire (conc e composizione)
Per capire in che condizioni si formano micelle sferiche
Uptake prvisione di un model drug per sapere il ‘carico’teorico
PLA idrofobico PEO idorfilico

## Slide 68: Objective: Effect of drug loading
Model drug: NIFEDIPINE (Adalat®, Nifedical®, Procardia®)
  Calcium channel blocker
    Ischemic cardiopathy
    Chronic arterial hypertension
    Raynaud syndrome
    Premature delivery
Highly hydrophobic and with side effects
  Needs delivery system
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753

## Slide 69: Diblock copolymer phase diagram
Phase diagram of diblock copolymers A-B
[Mean Field Theory - Leibler]
f = Volumetric fraction of one specie (A or B)
T
Classical phases:
LAMELLAR
HEXAGONAL (cylindrical)
SPHERICAL
Complex phases:
BICONTINUOUS (gyroid)
PERFORATED LAMELLAS
LAM
BCC
HEX
GYR
GYR
BCC
HEX
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753
Notes: In melt

## Slide 70: PLA-PEO AQUEOUS SOLUTION
Phase diagram derived from DPD simulations
Legend:
= micelles
= PLA spheres (SPLA)
= PEG spheres (SPEG)
= PLA cylinders (CPLA)
= PEG cylinders (CPEG)
= PLA perforated lamellas or gyroid phase (PLPLA/GPLA)
= Lamellas
= PEG perforated lamellas or gyroid phase (PLPEG/GPEG)
= disordered phase, lamellar micelles, cylindrical micelles..
v/v concentration in water
PLA fraction
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753
Notes: In acqua --- novità

## Slide 71: Predicted phase morphologies of PLA-PEO in water: F = 0.9 v/v
0.2
0.4
0.5
0.8
0.9
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753

## Slide 72: Predicted phase morphologies of PLA-PEO in water: F = 0.2 v/v
0.3
0.4
0.6
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753

## Slide 73: Predicted phase morphologies of PLA-PEO-PLA in water: fPLA = 0.57
0.10 %
0.15 %
0.22 %
0.35 %
0.50 %
0.60 %
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753

## Slide 74: Micelle loading with drug: PLA-PEO
0 %
4 %
12 %
22 %
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753
Drug concentration limit around 15%

## Slide 75: Micelle loading with drug: PLA-PEO-PLA
1 %
2 %
3 %
4 %
7 %
Posocco, Fermeglia, Pricl, J. Mater. Chem. 2010, 20, 7742-7753
Drug concentration limit around 2-3 %

## Slide 76: Outline of talk
Introduction
  Multiscale Molecular Modeling
Mapping procedure
  From atomistic simulation to mesoscale
  From mesoscale to micro FEM
Applications to nanostructured polymer systems
  Top down nanostructures
    Classical PCN
  Bottom up design
    Localization of gold nanoparticles in di-block copolymers
    Effect of chain length and grafting density
    Self assembly of nanostructures on gold nanoparticles
  Special applications
    Block copolymers for drug delivery
Conclusions
Notes: 76

## Slide 77: Conclusions
Message passing multiscale molecular modeling
  Mapping atomistic to mesoscale
  Mapping mesoscale morphology to microFEM
Useful for the design of nanostructured systems
  Interpretation and design of experiments
  Characterization of nanoparticle dispersion
Applied to nanostructured polymer system of industrial interest
  Automotive industry
  Opto electronic industry
  Polymer industry
  Nanomedicine & bio based economy
General design approach for nanostructured materials & systems

## Slide 78: Acknowledgments
Financial support:
  Nanomodel EU Project
  MULTIPRO EU Project
  Multihybrids EU Project
  GreenBoat Design, EU PorFesr
  NanoStata – Industry 2015
People & institutions
Sabrina Pricl
Radovan Toth
Paola Posocco
Erik Laurini
Paolo Cosoli
Daniel Romero
Simão P. Pereiraa
Francesca Santese
Valentina Dal Col
Domenico Marson
Tina Stokelj
Giulio Scocchi
Johannes G.E.M. Fraaije
Jan-Willem Handgraaf
Martin Lisal
Zbysek Posel
Nanomodel Partners
  Dave K. Smith, Anna Barnard & Simon P. Jones, University of York, U.K.
  Nathan P. Gabrielson & Daniel W. Pack, University of Illinois at Urbana Champaign, USA
  Chun-Ho Wong & Hak-Fun Chow, The Chinese University of Hong Kong
  Carlo V. Catapano, Anastasia Malek, IOSI, Bellinzona, Switzerland
  Aaron Tagliabue, Enzio Ragg, University of Milan
  Kostas Karatasos, University of Thessaloniki, Greece
  Lucia Pasquato, University of Trieste
  Sara Padovani, CRP-FIAT,
  Ling Peng group, CNRS, Marseille (F)
  MarcoPierotti, Elena Tamborini, Silvana Pilotti, NCI, Milan
  Giuseppe Mensitieri, University of Naples