## Slide 1: Laboratory Testing of Cement-based Materials to Support Durability Modelling
Angélique ROUSSELET
French Alternative Energies and Atomic Energy Commission (CEA), Paris-Saclay Centre
TC Regional Workshop on Approaches to Ageing Management of Waste Packages in Storage
Joint ICTP-IAEA Workshop on Degradation Modelling of Disposed Radioactive Wasteforms
18th – 22nd September 2023, Trieste (Italy)

## Slide 2: INTRODUCTION
Durability is the ability to maintain desired performances within a specified time frame.
Durability can be impacted by several processes:
Loss of performances of waste packages
Internal causes
AAR
DEF
Waste/matrix interaction
Radiolysis
External causes
Unsaturated
medium
Saturated medium

## Slide 3: INTRODUCTION
Unsaturated
medium
Saturated
medium
Gas transport:
  Drying
  Atmospheric carbonation
  Hydrogen transfer
Aqueous transport:
  Leaching of radionuclide
  Leaching of the cement material
  Reaction with ions from the environment

## Slide 4: INTRODUCTION
Acquisition of experimental data (laboratory testing)
Understanding the phenomenology
Modelling experimental data

## Slide 5: CONTENT
Leaching in pure water
Sulphate attack
Case study : interaction with Callovo-Oxfordian groundwater

## Slide 6: LEACHING IN PURE WATER
1

## Slide 7: LEACHING IN PURE WATER
Control of the composition of the leaching solution:
  pH: automatic titration to maintain a constant pH (7)
  Renewal of the leaching solution
  Protection from atmospheric CO2
  Control of the temperature
Unidirectional diffusion (lateral coating of the sample).
Experimental set-up
Pure water
Adapted from Planel et al. (2006) Cem.Conc.Res., 36:137-143.

## Slide 8: LEACHING IN PURE WATER
Chemical analysis of the leachate:
The cumulated amount of OH- is calculated from the volumes of acid added to maintain the constant pH of 7 :
Peycelon et al. (2006) REGC, 10:1107-1125.
Leaching of a CEM I cement paste at 25°C
: exposed surface of the sample in dm²
Cumulated amounts of other aqueous species (Ca, Si, Al, etc.) are determined thanks to the renewal of the leachate.

## Slide 9: LEACHING IN PURE WATER
Cumulated amounts are proportional to the square root of time
  typical of a process controlled by diffusion (2nd Fick law)
OH- is leached two times faster than [Ca2+]
  coherent with the dissolution of portlandite :
Peycelon et al. (2006) REGC, 10:1107-1125.
Leaching of a CEM I cement paste at 25°C
Chemical analysis of the leachate:

## Slide 10: LEACHING IN PURE WATER
Pure water is a strong decalcifying agent of cement-based materials :
  Visible zonation translating the progressive decalcification of the altered zones
1 . Superficial layer (enriched in aluminium and silicon) | 2. CSH | 3. CSH Ettringite | 4. CSH Ettringite Monosulfoaluminate | 5. Unaltered material CSH Ettringite Monosulfoaluminate Portlandite
1
2
3
4
5
Mainguy et al. (2000) Cem.Concr.Res 30:83-90.
Evolution of the mineralogy:

## Slide 11: LEACHING IN PURE WATER
Leaching of OPC materials in pure water is modelled considering the evolution of calcium only (since all major hydrates contain calcium (CH, CSH, AFm, AFt).
Simplified modelling
Inputs :
Initial concentration in the solid phase of Ca and Si
Initial porosity and coefficient of diffusion
Outputs :
Depth of degradation
Quantities of leached calcium

## Slide 12: LEACHING IN PURE WATER
Resolution of the mass balance equation for calcium only:
Simplified modelling
Diffusion of Ca governed by Fick’s law
Dissolution of Ca in the solid phase

## Slide 13: LEACHING IN PURE WATER
Relation between CCa and SCa is based on experimental data.
Simplified modelling
Faucon et al. (1998) Cem.Concr.Res., 28:847-857.
[Ca2+]=21mmol/l
Threshold due to portlandite dissolution
2<[Ca2+]<21mmol/l
Decalcification of C-S-H phase + progressive dissolution of AFm & AFt
[Ca2+]<2mmol/l
Solid phase is constituted of silica gel

## Slide 14: LEACHING IN PURE WATER
The evolution of porosity is linked to mineralogy.
Simplified modelling
Mainguy et al. (2000) Cem.Concr.Res., 30:83-90.
Increase of porosity due to the dissolution of portlandite
Increase of porosity due to the progressive dissolution of hydrates (AFm+AFt)
Initial porosity

## Slide 15: LEACHING IN PURE WATER
An empirical relation is established between porosity and coefficient of diffusion.
  Based on the determination of De in OPC pastes presenting different porosities (due to different w/c).
Simplified modelling
Mainguy et al. (2000) Cem.Concr.Res., 30:83-90.

## Slide 16: LEACHING IN PURE WATER
Outputs:
  No detail on the phase assemblage.
Simplified modelling
Mainguy et al. (2000) Cem.Concr.Res., 30:83-90.
Depth of degradation (mm) | 3 months | 6 months
Experiment | 1.45 | 2.1
Model | 1.4 | 2.0

## Slide 17: LEACHING IN PURE WATER
Chemical reactions
Hydrodynamic processes
Reactive transport modelling
Dissolution
and
Precipitation
Aqueous reactions
Redox reactions
Sorption
Etc.
Diffusion
and
Advection
Dispersion

## Slide 18: LEACHING IN PURE WATER
Reactive transport modelling
Leaching of OPC materials in pure water is modelled considering the all the elements (Ca, Si, Al, SO42-).
Chemical reactions
Hydrodynamic processes

## Slide 19: LEACHING IN PURE WATER
Reactive transport modelling
Variation of porosity calculated with the evolution of the mineralogy.
Variation of De calculated with an empirical relation.
  Example : modified Archie’s law
Chart: ω
| 0.01 | 0.02 | 0.04 | 0.06 | 0.08 | 0.1 | 0.12 | 0.14000000000000001 | 0.16 | 0.18 | 0.2 | 0.22 | 0.24 | 0.26 | 0.28000000000000003 | 0.3
a = 3 | 0 | 1.4579e-16 | 3.9364e-15 | 1.8224e-14 | 5.0007e-14 | 1.0628e-13 | 1.9405e-13 | 3.2031e-13 | 4.9205e-13 | 7.1629e-13 | 1e-12 | 1.3502e-12 | 1.7739e-12 | 2.278e-12 | 2.8697e-12 | 3.5558e-12
a = 2 | 0 | 2.7701e-15 | 2.4931e-14 | 6.9252e-14 | 1.3573e-13 | 2.2438e-13 | 3.3518e-13 | 4.6814e-13 | 6.2327e-13 | 8.0055e-13 | 1e-12 | 1.2216e-12 | 1.4654e-12 | 1.7313e-12 | 2.0194e-12 | 2.3296e-12
a = 1,5 | 0 | 1.2075e-14 | 6.2741e-14 | 1.35e-13 | 2.2362e-13 | 3.2601e-13 | 4.4051e-13 | 5.6596e-13 | 7.0147e-13 | 8.4634e-13 | 1e-12 | 1.162e-12 | 1.3319e-12 | 1.5093e-12 | 1.694e-12 | 1.8857e-12
a = 1 | 0 | 5.2632e-14 | 1.5789e-13 | 2.6316e-13 | 3.6842e-13 | 4.7368e-13 | 5.7895e-13 | 6.8421e-13 | 7.8947e-13 | 8.9474e-13 | 1e-12 | 1.1053e-12 | 1.2105e-12 | 1.3158e-12 | 1.4211e-12 | 1.5263e-12
Opening
Clogging
a : empirical fitting parameter

## Slide 20
Amount of Ca2+ released (mol/dm²/days1/2)
Cement | 25 °C |  | 50 °C |  | 85°C | 
 | Exp. | Mod. | Exp. | Mod. | Exp. | Mod.
CEM I | 0.0150 | 0.0152 | 0.028 | 0.027 | 0.046 | 0.045
CEM V | 0.0036 | 0.0031 | 0.0059 | 0.0057 | 0.0118 | 0.0126
85°C
85°C
50°C
50°C
25°C
25°C
Peycelon et al. (2006) REGC, 10:1107-1125.
CEM I
CEM V
LEACHING IN PURE WATER
Modelling the leachate composition:
Comparison between experimental data and model.
Possibility to take into account the effect of temperature.

## Slide 21: LEACHING IN PURE WATER
Impact of the opening of the porosity in the degraded zones :
  Input and fitting parameters (Archie’s law) :
    De(ω0) = 10-11m²/s
    ω0 = 0.2
    α = 2.8
  Decalcification of C-S-H :
    CSH1.8 → CSH1.1
Constant diffusion coefficient
Variable diffusion coefficient
Unaltered zone
Altered zone
1
2
Unaltered zone
Altered zone
1
2
van der Lee et al. (2008) ConMod’08
Modelling the mineralogical evolutions:

## Slide 22: LEACHING IN PURE WATER
Stora et al. (2009) Cem.Concr.Res., 39:763-772.
Unaltered zone
Altered zone
Altered zone
Unaltered zone
Simulated evolution of the Young modulus
Simulated mineral composition of a CEM I paste (w/c=0.4) leached for 50 days.
Input
  Modelling the evolutions of Young modulus E using experimental data on the different phases.
Chemo-mechanical modelling:

## Slide 23: SULPHATE ATTACK
2

## Slide 24: SULPHATE ATTACK
Ca2+
SO42-
Description of the general process:
Sodium sulfate
Portlandite
Gypsum
Monosulfate
Tricalcium
aluminate
Calcium aluminate phases
Ettringite
Two phenomena at play:
  Leaching from the material
  Mass transport of corrosive agents into the material

## Slide 25: SULPHATE ATTACK
Experimental set-up :
Planel et al. (2006) Cem.Conc.Res., 36:137-143.

## Slide 26: SULPHATE ATTACK
  Diffusion of sulphate ions in the material (negative flux)
  Fluxes of OH- are similar for leaching in H2O and Na2SO4
  Lower flux of Ca2+ in Na2SO4
    Ca2+ consumption
Planel et al. (2006) Cem.Conc.Res., 36:137-143.
Chemical analysis of the leachate:

## Slide 27: SULPHATE ATTACK
Mineralogy of the leached zone
Planel et al. (2006) Cem.Conc.Res., 36:137-143.
  Reaction of SO42- with Ca2+ and Al(OH)4- to precipitate ettringite and gypsum,
  Dissolution and precipitation fronts evolve as the square root of time (diffusion).

## Slide 28: SULPHATE ATTACK
Solid characterisation
(XRD)
(SEM)
Cracking due to internal pressure induced by mineral precipitation
  No cracks in zone 1 (interface with the leachate)
    Precipitation of ettringite, total dissolution of portlandite
  Major cracks in zone 2
    Formation of gypsum & ettringite, presence of portlandite
Planel et al. (2006) Cem.Conc.Res., 36:137-143.

## Slide 29: SULPHATE ATTACK
Modelling the mineralogical evolutions :
Experimental
(XRD)
Model
(HYTEC)
Planel (2002) Ph.D. Thesis
Counts
Depth (mm)
  Chemical-transport modelling of the evolution of the mineralogy of the cement paste

## Slide 30: SULPHATE ATTACK
From a chemical model to a mechanical model…
Cracking patterns
external surface
Time
Planel (2002) Ph.D. Thesis
  Numerical simulation of tensile damage with finite elements (CASTEM).
  The internal pressure is estimated according to the mineral volume variation :

## Slide 31: CASE STUDY : CALLOVO-OXFORDIAN GROUNDWATER
3

## Slide 32: Case study : COx groundwater
COx pore water composition :
 | Na | K | Ca | Mg | Sr | Cl | S | Si | Fe | Al | TIC*
mmol/l | 45.6 | 1 | 7.4 | 6.7 | 0.2 | 41 | 15.6 | 0.2 | 0.03 | 4.7.10-6 | 3.3
T (°C) | pH
25 | 7.1
*TIC : Total Inorganic Carbon
In the groundwater, TIC is imposed by a PCO2 30 times higher than atmospheric pressure.
Expected phenomena :
  Leaching (pH = 7.1)
  Sulphate attack
  Other reactants : CO32-, Mg2+

## Slide 33: Case study : COx groundwater
COx pore water composition :
 | Na | K | Ca | Mg | Sr | Cl | S | Si | Fe | Al | TIC*
mmol/l | 45.6 | 1 | 7.4 | 6.7 | 0.2 | 41 | 15.6 | 0.2 | 0.03 | 4.7.10-6 | 3.3
T (°C) | pH
25 | 7.1
*TIC : Total Inorganic Carbon
In the groundwater, TIC is imposed by a PCO2 30 times higher than atmospheric pressure.
Parameters to control in an experimental set-up :
  Temperature
  Composition of the solution :
    Renewal of the leachate
    PCO2

## Slide 34: Case study : COx groundwater
Experimental test in controlled conditions :
Dauzères et al. (2014) Cem.Concr.Res., 58:76-88.
  Control of the composition of the leaching solution :
  pH=7.1 and concentration in carbonates are maintained by controlling the flow of CO2.
  Renewal of the leaching solution to maintain the concentrations in other elements approximatively constant and avoid accumulation of leached species.

## Slide 35: Case study : COx groundwater
Results :
Leaching :
  dissolution of portlandite
2D Raman mapping of portlandite
XRD
Dauzères et al. (2014) Cem.Concr.Res., 58:76-88.

## Slide 36: Case study : COx groundwater
Results :
Sulphate attack :
  Precipitation of ettringite in the degraded zone
Elemental mapping (EDX)
Dauzères et al. (2014) Cem.Concr.Res., 58:76-88.

## Slide 37: Case study : COx groundwater
Results :
Action of carbonates and magnesium:
  Formation of a dense and magnesium-rich calcite crust on the surface of the sample.
Elemental mapping (EDX)
XRD
Raman mapping
of calcite
Dauzères et al. (2014) Cem.Concr.Res., 58:76-88.

## Slide 38: Case study : COx groundwater
Modelling the mineralogical evolutions :
Model in agreement with experimental results.
Adapted from Dauzères (2010) Ph.D. Thesis
Depth (µm)
(mol/l)
Ettringite precipitation
Portlandite
dissolution
Calcite
precipitation
C-S-H decalcification
Modelling at 5 months
Sound core

## Slide 39: Case study : COx groundwater
ω
Depth (µm)
j
k
m
l
m
Sound core
l
k
j
CaCO3
No Ca(OH)2
Ettringite precipitation
Dense calcite crust : low porosity (ω=0.06)
Competing effects : porosity opening (total dissolution of portlandite) vs. clogging (ettringite precipitation)
→ Overall, porosity opening
Ettringite precipitation : porosity clogging
Sound core (ω0=0.25)
Adapted from Dauzères (2010) Ph.D. Thesis
Effect of chemical transformation on porosity :
Modelling at 5 months

## Slide 40: Case study : COx groundwater
Depth (µm)
m
Sound core
l
k
j
CaCO3
No Ca(OH)2
Ettringite precipitation
Impact on ionic transport in the material :
Modelling at 5 months
Using an empirical law (such as modified Archie’s law)
    De(ω0) = 6.10-12m²/s
    ω0 = 0.25
    α = 3.5
Adapted from Dauzères (2010) Ph.D. Thesis

## Slide 41: SUMMURY
02
Modelling the experiment
Fitting of parameters on the experimental data :
  Coefficient of diffusion,
  Relation between porosity and the coefficient of diffusion,
  Etc.
Ensuring the validity of the input data used for modelling (thermodynamics database, initial chemical modelling of the material)
01
Acquisition of experimental data
Adaptive experimental set-up to test in different environments.
Control of different experimental parameters (temperature, geometry, composition of the leaching solutions) to facilitate modelling.
Identification of the fundamental mechanisms of alteration of the material.

## Slide 42
Angélique ROUSSELET
angelique.rousselet@cea.fr
CEA, Paris-Saclay Centre
DES/ISAS/DRMP/S2CM/LECBA
TC Regional Workshop on Approaches to Ageing Management of Waste Packages in Storage
Joint ICTP-IAEA Workshop on Degradation Modelling of Disposed Radioactive Wasteforms
18th – 22nd September 2023, Trieste (Italy)