## Slide 1: Cement Chemistry Modelling
Angélique ROUSSELET
French Alternative Energies and Atomic Energy Commission (CEA), Paris-Saclay Centre
TC Regional Workshop on Approaches to Ageing Management of Waste Packages in Storage
Joint ICTP-IAEA Workshop on Degradation Modelling of Disposed Radioactive Wasteforms
18th – 22nd September 2023, Trieste (Italy)

## Slide 2: INTRODUCTION
Two approaches:
  Microstructure modelling
  Thermodynamic modelling
Both approaches can require some input data which can be calculated:
  Degree of hydration of cement
  Alkali concentrations and pH of the pore solution
Modelling the chemistry of cement materials:

## Slide 3: CONTENT
Input parameters
  Degree of hydration
  Alkali concentrations and pH
Microstructure modelling of the cement paste
  Powers & Brownyard model
  Jennings & Tennis model
Thermodynamic modelling
  Equilibrium constant method
  Gibbs energy minimization
  Long-term behaviour of cement materials

## Slide 4: Input parameters
1

## Slide 5: INPUT PARAMETERS
Degree of hydration = weight fraction of cement and individual clinker phases which have fully reacted at a given time.
Two common kinetic models are available for cement materials:
  Use of an Avrami type equation
  Parrott & Killoh model of hydration
Both models rely on empirical data.
Calculating the degree of hydration

## Slide 6: INPUT PARAMETERS
The equation describes how solids transform from one phase into another at constant temperature.
It’s use for Portland cement was introduced by Dalziel & Gutteridge (1986).
  Fraction of reacted phase, F, is a function of time, t.
  Parameters , and are fitted on a set of experimental data.
Avrami type equation
Chart: Time (days)

## Slide 7: INPUT PARAMETERS
A set of empirical equations is used to describe the different mechanisms involved in hydration:
Parrott & Killoh model
  Degree of hydration:
  Rate of nucleation and growth:
  Rate of diffusion:
  Rate of secondary shell formation:
At each time step t, the lowest value of R (controlling rate) is selected for the calculation of .

## Slide 8: INPUT PARAMETERS
A critical value of degree of hydration is introduced in order to translate the observation that the rate of hydration is reduces at later ages and for materials of low .
  Critical degree of hydration :
    If
    If
Parrott & Killoh model
The impact of the relative humidity is also taken into account using the following factor :

## Slide 9: INPUT PARAMETERS
Parrott & Killoh model
 | K1 | N1 | K2 | K3 | N3
C3S | 1,5 | 0,7 | 0,05 | 1,1 | ,3,
C2S | 0,5 | 1,0 | 0,006 | 0,2 | 5,0
C3A | 1,0 | 0,85 | 0,04 | 1,0 | 3,2
C4AF | 0,37 | 0,7 | 0,015 | 0,4 | 3,7
Parrott & Killoh (1986)
Empirical constants for Portland cement at ambient temperature for each clinker phases:
Chart: Time (days)

## Slide 10: INPUT PARAMETERS
The model was developed for Portland cement (Taylor, 1987).
It relies on empirical data and takes into account the sorption of alkalis by cement hydrates.
Alkali concentrations and pH
Inputs :
Initial water to cement ratio ()
Global degree of hydration
  Experimental of calculated
Outputs :
Alkali and hydroxyl concentrations in pore solution
pH of the pore solution

## Slide 11: INPUT PARAMETERS
Alkali concentrations and pH
Quantity of alkalis released by the cement
Quantity of alkalis released by the cement
𝑛_𝑟𝑒𝑙𝑒𝑎𝑠𝑒𝑑=𝑛_(𝑝𝑜𝑟𝑒 𝑠𝑜𝑙𝑢𝑡𝑖𝑜𝑛)+𝑛_𝑠𝑜𝑟𝑏𝑒𝑑
Alkalis in the pore solution
Alkalis in the pore solution
𝑛_(𝑝𝑜𝑟𝑒 𝑠𝑜𝑙𝑢𝑡𝑖𝑜𝑛)=𝐶×𝑉_(𝑝𝑜𝑟𝑒 𝑠𝑜𝑙𝑢𝑡𝑖𝑜𝑛)
Alkalis taken up by cement hydrates
Alkalis taken up by cement hydrates
𝑛_𝑠𝑜𝑟𝑏𝑒𝑑=𝑏×𝑃×𝐶
The volume of reacted water is fitted empirically.
𝑉_(𝑝𝑜𝑟𝑒 𝑠𝑜𝑙𝑢𝑡𝑖𝑜𝑛)= 𝑉_(𝑖𝑛𝑖𝑡𝑖𝑎𝑙 𝑤𝑎𝑡𝑒𝑟)−𝑉_(𝑟𝑒𝑎𝑐𝑡𝑒𝑑 𝑤𝑎𝑡𝑒𝑟)
The volume of reacted water is fitted empirically.
1/ Binding factors, b, are determined empirically.
2/ The ratio of relevant hydration products, P, is fitted empirically.
1/ Binding factors, b, are determined empirically.
2/ The ratio of relevant hydration products, P, is fitted empirically.

## Slide 12: INPUT PARAMETERS
Alkalis are present in the clinker in:
  Sulphate phases
    These alkalis are considered readily soluble.
    By default, assumption that 35% of the total Na2O content and 70% of the total K2O content.
  Hydraulic phases
    By default, a distribution of alkalis typical of Portland clinker is assumed.
    Hydration degree is applied to each hydraulic phases.
Alkali concentrations and pH
Weight fractions | Na2O | K2O
C3S | 0.44 | 0.29
C2S | 0.17 | 0.41
C3A | 0.36 | 0.27
C4AF | 0.03 | 0.03
Total | 1 | 1
Distribution of alkalis in the hydraulic phases of a Portland clinker provided by Taylor.
Taylor (1987) Adv.Cem.Res., 1:5-17.

## Slide 13: INPUT PARAMETERS
The empirical equation of Dalziel & Gutteridge (1986) is employed to determine the degree of reaction of hydraulic phases.
  The D&G equation is also employed to fit the weight fraction of reacted water ( and the quantity of hydrates relevant for alkali sorption ().
Alkali concentrations and pH
 | k1 | k2 | k3
Reacted water | 0.25 | 0.69 | 0.90
P | 0.25 | 0.56 | 0.90
Taylor (1987) Adv.Cem.Res., 1:5-17.

## Slide 14: INPUT PARAMETERS
Alkali concentrations and pH
Caution : the empirical parameters were fitted for an average Portland cement
    C3S (60 wt%), C2S (15 wt%), C3A (8 wt%), C4AF (10 wt%)
Following other empirical equations, a value of pH can be determined :
Chart: w/c
| 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
[Na+] | 0.21982 | 0.18678 | 0.16237 | 0.14361 | 0.12873 | 0.11665 | 0.10664 | 0.09821 | 0.091016 | 0.084805 | 0.079387 | 0.07462 | 0.070393 | 0.066619 | 0.06323
[K+] | 0.68081 | 0.5342 | 0.43955 | 0.37339 | 0.32454 | 0.28699 | 0.25724 | 0.23307 | 0.21305 | 0.1962 | 0.18182 | 0.1694 | 0.15858 | 0.14905 | 0.1406
pH | 13.9049 | 13.8186 | 13.747 | 13.6857 | 13.6321 | 13.5844 | 13.5416 | 13.5026 | 13.4668 | 13.4338 | 13.4032 | 13.3745 | 13.3477 | 13.3224 | 13.2985

## Slide 15: Microstructure modelling
2

## Slide 16: MICROSTRUCTURE MODELLING
Principle : cement hydrates can only form if they have enough space to do so.
Several models have been developed after the pioneer work of Powers.
Different models :
  Simplified Powers (requires minimal input parameters)
  Extensive Powers
  Jennings & Tennis
Microstructure models are volumetric models.

## Slide 17: MICROSTRUCTURE MODELLING
The initial volume of water (w0) and cement (c0) is equal to the volume of the hardened cement paste (hcp).
The hardened cement paste is constituted of :
    Unreacted cement (unreact)
    Hydration products (hp)
      Contain hydrates and gel porosity
    Capillary space (cp)
Fundamentals of the Powers & Brownyard model
Chart: Volumes (%)
Cement | 44.2478 | 4.8633 | 4.8633 | 4.8633
Water | 55.7522
Hydration products | 86.5174
Hydrated cement | 63.1577 | 63.1577
Gel water | 23.3597
Capillary porosity | 8.6192 | 8.6192
Total porosity | 31.979
t=0
Hardened cement paste
C0
W0
Hydrated products
unreact
Hydrates
Gel por.
cp
cp
Total por.
Hydrates

## Slide 18: MICROSTRUCTURE MODELLING
Fundamentals of the Powers & Brownyard model
Evaporable
water
Free water in capillary space
Gel water retained by hydrated products
Non evaporable water
Water chemically bound within cement hydrates
Model based on extensive experimental work on the quantification of water:
Water retained after P-drying.
Water only removed by ignition.
Constitute a measure of degree of hydration
Adsorption
isotherms
Water removed by P-drying

## Slide 19: MICROSTRUCTURE MODELLING
Hydrated products:
  Individual hydrates (CH, C-S-H, AFm, AFt, etc.) are not considered.
  Include hydrates (h) and gel porosity (gp).
  Gel porosity or gel water is mostly due to the properties of the C-S-H phase :
    Non chemically bound water adsorbed on C-S-H or contained in the (nano)porosity of C-S-H.
Fundamentals of the Powers & Brownyard model
Kurdowski (2014) Cement & Concrete Chemistry, ISBN 978-94-007-7944-0.

## Slide 20: MICROSTRUCTURE MODELLING
Unreacted cement:
  Depends on the degree of hydration of the cement.
  In Powers’ original work, the degree of hydration considered was determined experimentally, but it can also be calculated.
Capillary space:
  Remnant of the initially water-filled space:
    Unreacted water (free water) present in the paste porosity,
    Chemical shrinkage.
Fundamentals of the Powers & Brownyard model

## Slide 21: MICROSTRUCTURE MODELLING
Developed and applicable only for Portland cement.
Simplified Powers
Inputs :
Initial water to cement ratio ()
Global degree of hydration
Outputs :
Volume of hydrated products and gel porosity
Volume of capillary space (& total porosity)

## Slide 22: MICROSTRUCTURE MODELLING
Volume of hardened cement paste
Simplified Powers
= 0.317
3.15 kg/l
= 0.317 ()
Volume of unreacted cement

## Slide 23: MICROSTRUCTURE MODELLING
Evaporable water as a function of total water content for different pastes (different and curing time) in saturated conditions.
  Break at ( )
  : the paste has reached maximum hydration
  0,38 is therefore a critical value later referred to as (w/c)*
Simplified Powers
Chart: wtot/c0
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.44 | 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.44
 | 0 | 0.0482 | 0.0964 | 0.1446 | 0.1928 | 0.21208
 | 0.213 | 0.273 | 0.373 | 0.473 | 0.573 | 0.673 | 0.773

## Slide 24: MICROSTRUCTURE MODELLING
Simplified Powers
= 0.697
Volume of capillary space
Volume of hydration products
Volume of gel porosity experimentally determined to be 28% of the volume of hydrated products:
Chart: Degree of hydration
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
Vunreact | 44.212 | 39.7908 | 35.3696 | 30.9484 | 26.5272 | 22.106 | 17.6848 | 13.2636 | 8.8424 | 4.4212 | 0
Vhc | 0 | 7.0964 | 14.1927 | 21.2891 | 28.3855 | 35.4819 | 42.5782 | 49.6746 | 56.771 | 63.8674 | 70.9637
Vgp | 0 | 2.6247 | 5.2494 | 7.8741 | 10.4987 | 13.1234 | 15.7481 | 18.3728 | 20.9975 | 23.6222 | 26.2469
Vcp | 55.788 | 50.4881 | 45.1883 | 39.8884 | 34.5886 | 29.2887 | 23.9888 | 18.689 | 13.3891 | 8.0893 | 2.7894
Hydrates
Gel por.
Capillary space
Unreacted cement

## Slide 25: MICROSTRUCTURE MODELLING
Distinction between the volume of free water and the volume left due to chemical shrinkage:
  Cp = fw + shr
Extensive Powers
Inputs :
Cement composition
Initial water to cement ratio ()
Global degree of hydration
Outputs :
Volume of hydrated products and gel porosity
Volume of capillary space
Chemical shrinkage

## Slide 26: MICROSTRUCTURE MODELLING
Extensive Powers
Chart: Volume fractions
| t=0 | Hardened cement paste | Hardened cement paste
Cement | 43.9367 | 6.1511 | 6.1511
Hydrated products | 73.9359
Hydrated cement | 54.1827
Gel porosity | 19.7533
Water | 56.0633 | 11.3415
Shrinkage | 8.5714
Capillary volume | 19.9129
t=0
Hardened cement paste
C0
W0
Shr.
fw
Hydrated products
C
Hydrated cement
Gel por.
Cap. Vol.
The change of volume due to hydration is taken into account via the densities of reacted water.
  Density of non evaporable water () and gel water () are lower than 1.
Quantities of non evaporable and gel water were experimentally fitted to the composition of the clinkers.

## Slide 27: MICROSTRUCTURE MODELLING
Volume of hydrated products
Extensive Powers
& are determined experimentally.
Weight fractions of non evaporable and gel water:
: weight fraction of phases in the clinker
: weight of reacted water
: weight of reacted cement

## Slide 28: MICROSTRUCTURE MODELLING
Extensive Powers
Volume of free water
Volume due to shrinkage
Chart: Degree of hydration
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
Vunreact | 43.9367 | 39.5431 | 35.1494 | 30.7557 | 26.362 | 21.9684 | 17.5747 | 13.181 | 8.7873 | 4.3937 | 0
Vhc | 0 | 6.3003 | 12.6006 | 18.9009 | 25.2012 | 31.5015 | 37.8019 | 44.1022 | 50.4025 | 56.7028 | 63.0031
Vgp | 0 | 2.2969 | 4.5938 | 6.8907 | 9.1876 | 11.4845 | 13.7813 | 16.0782 | 18.3751 | 20.672 | 22.9689
Vfw | 56.0633 | 50.8631 | 45.6629 | 40.4626 | 35.2624 | 30.0622 | 24.862 | 19.6618 | 14.4616 | 9.2614 | 4.0612
Vshr | 0 | 0.99668 | 1.9934 | 2.99 | 3.9867 | 4.9834 | 5.9801 | 6.9768 | 7.9734 | 8.9701 | 9.9668
Hydrates
Gel por.
Free water
Unreacted cement
Shr.

## Slide 29: MICROSTRUCTURE MODELLING
Access to the volume fractions of individual hydrates.
Jennings & Tennis
Inputs :
Initial water to cement ratio ()
Degrees of hydration of individual phases
Cement composition
Outputs :
Volume of C-S-H, C-S-H gel porosity, CH and AFm
Volume of capillary space (& total porosity)

## Slide 30: MICROSTRUCTURE MODELLING
Jennings & Tennis
Calculates the volumes of individual hydrates using a set of chemical reactions:
The model assimilates the AFt phase to the AFm phase because of their similar densities (1,77 and 1,99 respectively).
  Hydration of calcium silicate phases
  Hydration of aluminate and ferrite phases
(AFm)
(AFt)

## Slide 31: MICROSTRUCTURE MODELLING
Jennings & Tennis
Volume of portlandite (CH):
1.3 and 0.3)
are the molecular weight of compounds i
are the specific weight of compounds i
are the individual degree of hydration of phase i
are the weight percentage of compounds i in the cement

## Slide 32: MICROSTRUCTURE MODELLING
Jennings & Tennis
Volume of AFm:
Volume of C-S-H (excluding gel porosity):

## Slide 33: MICROSTRUCTURE MODELLING
Capillary space :
  Calculated by taking into account the increase of volume of each anhydrous phases due hydration.
  Increase of volume, , is calculated based on the hydration reactions.
Jennings & Tennis
Phases | (cm3/g)
C3S | 0.437
C2S | 0.503
C3A | 0.397
C4AF | 0.136
Phases | 
C3S | 0.437
C2S | 0.503
C3A | 0.397
C4AF | 0.136
Gel porosity:
  Based on new experimental data on C-S-H.

## Slide 34: MICROSTRUCTURE MODELLING
Output
Jennings & Tennis
Chart: Degree of hydration
| 0 | 9.9219737391783594E-2 | 0.20275915093248165 | 0.30011602526918624 | 0.39983260114634056 | 0.50341526490427957 | 0.60494747242944158 | 0.6951089391127101 | 0.80453353215904178 | 0.90495690451249733 | 0.99919516717130186
Vunreac | 43.9367 | 39.5773 | 35.0282 | 30.7506 | 26.3694 | 21.8183 | 17.3573 | 13.3959 | 8.5882 | 4.1759 | 0.035362
VCH | 0 | 1.878 | 4.1436 | 6.2402 | 8.3293 | 10.4052 | 12.3331 | 13.951 | 15.7864 | 17.3413 | 18.7402
VAFm | 0 | 0.76378 | 1.947 | 3.1093 | 4.2892 | 5.4472 | 6.4819 | 7.2999 | 8.1455 | 8.7665 | 9.2479
VCSH,dry | 0 | 3.6514 | 7.0233 | 10.1877 | 13.4726 | 16.9851 | 20.5551 | 23.8439 | 28.0022 | 31.9899 | 35.8092
Vgp | 0 | 2.0715 | 3.9845 | 5.7797 | 7.6433 | 9.6361 | 11.6614 | 13.5272 | 15.8863 | 18.1487 | 20.3154
Vcp | 56.0633 | 52.0579 | 47.8735 | 43.9324 | 39.8961 | 35.7081 | 31.6111 | 27.9821 | 23.5914 | 19.5778 | 15.8519
CH
Gel por.
Capillary
volume
Unreacted cement
AFm
CSH

## Slide 35: Thermodynamic modelling
3

## Slide 36: THERMODYNAMIC MODELLING
Resolution of mass action equations : “equilibrium constant method”
  Geochemical codes : PHREEQC (freeware), EQ3/6 (freeware), CHESS, MINTEQ (freeware).
Minimization of the Gibbs free energy of the system
  Geochemical codes: GEMS (freeware), web application CemGEMS (free)
Both approaches lead to similar results but require different inputs:
  No a priori assumptions on the phase assemblage and pH of the pore solution is needed with the minimization of the Gibbs free energy.
Two approaches are available to compute the thermodynamic equilibrium of a system

## Slide 37: THERMODYNAMIC MODELLING
Both approaches rely on the same thermodynamic data :
Two approaches are available to compute the thermodynamic equilibrium of a system
Relies on an extensive set of thermodynamic data for solid, liquid and gaseous phases.

## Slide 38: THERMODYNAMIC MODELLING
Must be as complete and as accurate as possible.
Thermodynamic database
Exemple : Thermoddem database (thermoddem.brgm.fr)
Thermodynamic constant K (solubility)
Temperature dependence of K

## Slide 39: THERMODYNAMIC MODELLING
Must be as complete and as accurate as possible.
Thermodynamic database
Exemple : Thermoddem database (thermoddem.brgm.fr)
Aqueous species to consider:
Gaseous species to consider:
Exemple of species needed in the database for atmospheric carbonation of portlandite:

## Slide 40: THERMODYNAMIC MODELLING
Requires a priori knowledge of the conditions (pH of equilibrium) and final phase assemblage.
Equilibrium constant method
Example : Determination of the phase assemblage of a Portland cement with CHESS using the thermoddem database.
Jaffeite (calcium silicate hydroxide)
Calcite
Monocarboaluminate
Jennite (crystalline C-S-H)
Ettringite
Clinochlore (chlorite)
Without exclusions to the database
With exclusions to the database
Portlandite
Calcite
Monocarboaluminate
C1.6SH
Ettringite
Hydrotalcite

## Slide 41: THERMODYNAMIC MODELLING
Modelling the phase assemblage of a Portland cement paste with Vminteq 4.0
Equilibrium constant method
Inputs:
Ca2+, H4SiO4, Al3+, SO42-, CO3- concentrations calculated from cement composition and its degree of hydration.
Na+, K+, pH calculated
Selection of possible phases allowed to precipitate
Outputs:

## Slide 42: THERMODYNAMIC MODELLING
Modelling the phase assemblage of a Portland cement paste with Vminteq 4.0
Equilibrium constant method
Outputs:
Results expressed as volume of minerals per volume of cement material:
 | Volume (%)
Unreacted cement | 8.3
C1.6SH | 36.5
Portlandite | 18.4
Ettringite | 4.0
Monocarboaluminate | 3.9
Hydrotalcite | 1.3
Calcite | 1.0
Porosity | 26.6

## Slide 43: THERMODYNAMIC MODELLING
Modelling with CemGEMS web application (https://cemgems.org/)
GEMS approach
Inputs:
Detailed cement composition.
Outputs :
Phase assemblage (C-S-H, CH, AFm, AFt, etc.)
Porosity
Composition of the pore solution
Kinetics of hydration

## Slide 44: THERMODYNAMIC MODELLING
Modelling with CEMGEMS web application
GEMS approach
Results expressed as volume of minerals per volume of cement material:
 | Volume (%)
Unreacted cement | 7.7
C1.6SH | 32.4
Portlandite | 16.3
Ettringite | 6.8
Monocarboaluminate | 0.6
Hydrotalcite | 2.4
Calcite | 1.5
Porosity | 29.0
Pore water
C-S-H
CH
AFt
C3S
C2S

## Slide 45: THERMODYNAMIC MODELLING
Two approaches:
Modelling long-term behaviour of waste forms and packages
Mixing tank:
Evolution with time of the total quantities of hydrated cement and encapsulated waste.
No spatial resolution
Reactive transport modelling:
Spatial resolution
Hydrodynamic processes are accounted for (diffusion, advection)

## Slide 46: THERMODYNAMIC MODELLING
Waste form from decommissioning of nuclear power plant was chosen as a model waste form.
Composition:
    Cement + Water + Additions (silica fumes, clinoptilolite) + Sand (quartz)
    Organic waste
    Metallic waste
Mixing tank approach
Wieland et al. (2020) Appl.Geochem., 115:104539.

## Slide 47: THERMODYNAMIC MODELLING
Kinetics laws are used to model:
  Degradation of organic matter (gas production and aqueous product of degradation)
  Metal corrosion
  Dissolution of quartz sand for neutral and alkaline conditions
Thermodynamic calculations to model chemical evolutions due to the degradation of waste.
Mixing tank approach
Wieland et al. (2020) Appl.Geochem., 115:104539.

## Slide 48: THERMODYNAMIC MODELLING
Spatial resolution.
Hydrodynamic processes (diffusion, dispersion and permeability of the material, advection).
  Chloride ingress within a Portland cement mortar at 180d.
Reactive transport modelling
Sharmilan et al. (2022) Cem.Concr.Res., 159:106861.

## Slide 49
Angélique ROUSSELET
angelique.rousselet@cea.fr
CEA, Paris-Saclay Centre
DES/ISAS/DRMP/S2CM/LECBA
TC Regional Workshop on Approaches to Ageing Management of Waste Packages in Storage
Joint ICTP-IAEA Workshop on Degradation Modelling of Disposed Radioactive Wasteforms
18th – 22nd September 2023, Trieste (Italy)