## Slide 1
Organic and Bio-organic Semiconductors
For Solar Energy and CO2 Reduction
Niyazi Serdar SARICIFTCI
Linz Institute for Organic Solar Cells (LIOS),
Institute for Physical Chemistry, Johannes Kepler University Linz, Austria
www.lios.at
e-
Trieste Lecture 22nd of May, 2014

## Slide 2
Happy Life
e-

## Slide 3
Our planet will be warmer
e-

## Slide 4
Can we get rid of CO2?
e-

## Slide 5
RECYCLING CO2
e-
Methanol as carrier and storage of energy
a.) Methanol can be mixed to gasoline
b.) Methanol is used in fuel cells
c.) Methanol is starting chemical for
Many other derivatives
George Olah, Nobel Prize 1994
Univ. of Southern California, USA

## Slide 6
Semiconducting Polymer “Inks”
e-

## Slide 7
Color Variations: Band Gap Engineering
e-

## Slide 8
Semiconducting and Metallic Polymers
---for they combine the electronic properties of metals and semiconductors
and
the processablity, synthesis advantages and flexibility of polymers..
e-

## Slide 9
Full Color Plastic Flat Panel Displays
e-

## Slide 10
White OLEDs by Lumiotech, Yonezawa
e-

## Slide 11
Ultrathin PLEDs
e-

## Slide 12
Encapsulation
Novaplasma Inc.,
Montreal, Canada
G. Dennler et al, 2005

## Slide 13: Roll to roll produced solar cells
Konarka Inc.

## Slide 14
Outdoor Demonstrations

## Slide 15: Ultrathin, shrinkable, strechable organic solar cells
Martin Kaltenbrunner, Matthew White et al. Nature Comm. DOI: 10.1038/ncomms1772 April, 2012

## Slide 17: Textile integrated organic solar cells fibers
Ayse Bedeloglu et al, Textile Research Journal (2009)

## Slide 18: Solar cell integrated textiles
A commercial solar jacket and bag
(www.scottevest.com, www.neubers.de )

## Slide 19
Small Molecular
Organic Solar Cells
“Tang- Cell“
C. W. Tang
Appl.Phys. Lett. 48(86)183
e-

## Slide 20
Tang Patents in KODAK
e-

## Slide 21
e-
-3
-3.5
-4
-4.5
-5
-5.5
[eV] vs vacuum
-6
HOMO
HOMO
LUMO
LUMO
ITO
PEDOT
PSS
Al
DONOR
“P"
ACCEPTOR
“N"
WORKING PRINCIPLE
Bi-layer polymer solar cells

## Slide 22
PCBM
MDMO-PPV
+
-
Light
ITO
Plastic foil
Aluminum
P EDOT-PSS
Organic Solar Cell Device Geometries
PCBM
+
-
MDMO-PPV
Light
ITO
Plastic foil
Aluminum
PEDOT-PSS
BILAYER
BULK HETEROJUNCTION
e-
Notes: Conjugated polymer/fullerene plastic solar cells of the first generation were consisting of two distinct layers, made of the donor polymer and the acceptor fullerene, respectively, sandwiched between two metal contacts. By mixing the polymer and fullerene components, thus replacing a single and flat junction by an interpenetrating network bulk-heterojunction, the device efficiency was dramatically improved.

## Slide 23
Photoinduced Charge Generation
An ultrafast e- transfer occurs between Conjugated Polymer / Fullerene composites upon illumination. The transition time is less than 40 fs. The Internal Quantum efficiency of charge generation is therefore ~100%.
MDMO PPV
3,7 - dimethyloctyloxy methyloxy PPV
PCBM
1-(3-methoxycarbonyl) propyl-1-phenyl [6,6]C61
DONOR
ACCEPTOR
N. S. Sariciftci, L. Smilowitz, A. J. Heeger and F. Wudl., Science 258, 1474 (1992)
e-

## Slide 25
Sariciftci Heeger Patents at UCSB
e-

## Slide 26
Sariciftci Heeger Patents at UCSB
e-
Birth of Bulk Heterojunction, 1992
Definition

## Slide 27
Color Variations: Band Gap Engineering
e-

## Slide 28
e-
Are our concepts working?

## Slide 29
1.) Light absorption
2.) Exciton diffusion
3.) Photoinduced electron transfer (exciton dissociation)
4.) Charge carrier transport (charge carrier recombination)
5.)Charge carrier collection at the electrodes (interface engineering)
Critical Steps for the Organic Photovoltaic Devices
e-

## Slide 30
Photon Harvesting
e-

## Slide 31
H. Y. Chen, J. H. Hou, et al., Nature Photonics, 2009, 3, 649-653.
J. H. Hou, et al., J. Am. Chem. Soc., 2009, 131, 15586–15587.
Yongye Liang, et al., J. Am. Chem. Soc., 2009, 131, 56–57
Yongye Liang, et al., J. Am. Chem. Soc. 2009, 131, 7792-7799

## Slide 32
Photon Harvesting Problem
Incident Photon to Electron Conversion efficiency:
e-
By low band gap materials we are loosing the green-blue region

## Slide 33
Energy Transfer Cascades
2 Förster resonant energy transfer cascade
3 charge transfer + transport
Inspired by photosynthesis
- R. Koeppe, O. Bossart, G. Calzaferri, and N.S. Sariciftci, Sol. Energ. Mater. Sol. Cells. 91(11); 986-995 (2007)
1 Light absorption
e-

## Slide 34
Tandem Solar Cells
Organic tandem solar cells:
Glass
Polymer:PCBM solar cell
ZnPc:C60 solar cell
Aluminium electrode
transparent ITO electrode
noncontinuous recombination layer
G. Dennler, H.-J. Prall, R. Koeppe, M. Egginger, R. Autengruber, N.S. Sariciftci, APL 89 (2006), 073502-1
e-

## Slide 35
Origin of the Open Circuit Voltage Voc

## Slide 36
Voc of Organic Solar Cells
e-

## Slide 37
Voc vs LUMO of Acceptor
Brabec et al., Advanced Functional Materials (2001), 11, No.5, 374-380
.
e-

## Slide 38
Voc vs HOMO of the Polymer Donor
Kwanghee Lee et al, Pusan Univ. Korea
p-DMOP-co-MEH-PPV (7:3)
4.9 eV
2.8 eV
5.42 eV
5.44 eV
3.08 eV
3.31 eV
3.9 eV
MEH-PPV
p-DMOP-PPV
C60 LUMO
1
2
3
Δ
High PL Quantum Efficiency Materials
High Ionization Potential Materials
Δ : Ip – LUMO level of C60
 | 1 | 2 | 3
Q.E. | 10% | 40% | 23%
e-

## Slide 39
Voc vs HOMO of the Polymer Donor
e-
Markus Scharber et al, Adv. Mater. 18 (2006) 789

## Slide 40
Nanomorphology of the
donor-acceptor composites

## Slide 41
Bulk Heterojunction Device Structure
Rene Janssen et al, 2004

## Slide 42
Morphology Effects-TEM Studies
Tom Martens, Jean Manca et al, 2003.
Solvent effects on the
nanoparticle dimensions

## Slide 43
Nanomorphology Effects-SEM Studies
Harald Hoppe et al. Adv. Func. Mater. 14, (2004) 1005,
Notes: Side view of the cross section of MDMO-PPV:PCBM blended films with varying mixing ratios (by weight). For the ratios 1:4, 1:3 and 1:2 the spherical clusters in the form of discs are clearly visibly surrounded by another phase, that contains smaller spheres of about 30-40 nm in size. For the 1:1 mixing ratio only these smaller clusters are found. The magnifications are 100 000 for the 1:4 and 1:3 ratio and 150 000 for the 1:2 and 200 000 for the 1:1 ratio.

## Slide 44
Morphology: Solvent effects
*S.E. Shaheen, C.J. Brabec, N.S. Sariciftci, F. Padinger, T. Fromherz, J.C. Hummelen, Appl. Phys. Lett. 78, 841 (2001)
A 2-3 fold increase of the IPCE and short circuit current was observed by S.E. Shaheen et al.* due to the change from toluene to chlorobenzene as solvent, while by AFM measurements a decrease in the surface roughness was detected.

## Slide 45
Bulk Heterojunctions: Revised

## Slide 46
Property Optimization
Structure
Property
Nanomorphology
Self Organization
Interchain
(Intermolecular)
Interactions
Molecular Structure
Molecular Engineering

## Slide 47: „Optimum“ Geometry for Organic and Hybrid Solar Cells
Organic n-type
conductor
(acceptor)
Low workfunction
electrode
Organic p-type
conductor (donor)
High workfunction
electrode
e-

## Slide 48
10 % Solar Cells (2011)
e-
Aramaki et al,
Mitsubishi Chemicals Labs, Tokyo

## Slide 49
D-A block copolymers
PCE ＝1.50%
Voc = 0.87 V;
Isc = 4.49 mA/cm2;
FF = 0.38
[Y. H. Geng, et al., J. Am. Chem. Soc., 2009, 131, 13242–13243]
e-

## Slide 50
Supramolecular Ordering
Di-block copolymer miscelle formation encapsulating fullerenes.
S. Jenekhe, & Chen,
Science 279, 1903 (1998)
e-

## Slide 51
Percolation Problem in Composites
Metal
Electrode
Metal
Electrode
Both donor and acceptor phases have to be percolated !!!
Fullerene (acceptor)
Conjugated Polymer (donor)
e-

## Slide 52
The ideal double-cable polymers…
acceptor
spacer
donor backbone
e-
h+
- ambipolar
perculation at low
concentration in
guest-host systems
Defined D-A interaction
and no phase separation
e-
Notes: Based on this finding, we became interested on the preparation of intrinsic ambipolar material, which we call double cables, consisting of a donor conjugated backbone carrying, via sigma-bond spacers, contiguos electron acceptor units.
Such a primary structure should represent a powerful way to control the donor/acceptor interaction, for instance by choosing spacers of a proper lenght, and should prevent phase separation. In the light of the results I have showed before, these expected properties are indeed interesting for the preparation of polymeric photovoltaic devices.
In addition, double-cables should be of interest as intrinsic ambipolar materials or polymeric rectifiers.

## Slide 53
The double-cable concept
e-
h+
e-

## Slide 54
Bio-Degradable Electronics
e-
Electronic waste is a great challenge
Textile integrated electronics and/or smart packages will
increase the volume of electronic waste in future
Biocompatible and biodegradable electronic materials are needed
In vivo electronics in biomedical research needs
bio-compatible electronic materials

## Slide 55
55
„From Consumer Electronics to
Consumable Electronics“
As of today: 5.6 billion cell phones are in use in the world
e-

## Slide 56: North Pacific Garbage Patch
e-

## Slide 57
Plastic abundance: 45,000 items/km2
Depth: up to 10 meters
1 million seabirds and 100,000 marine mammals killed each year
Global production of plastic: 260 million tons (2009)
Source: Telegraph UK, April 24, 2009
e-

## Slide 58
Glucose
Sucrose
Lactose
Caffeine
-carotene
e-

## Slide 59: Glucose / -carotene OFET
Mihai Irimia-Vladu, et al. 2009
e-

## Slide 60: Glucose + Caffeine / -carotene OFET
Adding caffeine into glucose improves the on-off ratio and lowers the operating voltage of the transistors !!!
Mihai Irimia-Vladu, et al. 2009
e-

## Slide 61
e-

## Slide 62: Shellac is a natural copolymer produced by the female lac beetle
200,000 female lac bugs
to produce 1 kg of shellac
Shellac is harvested from trees’ bark in India and Thailand
Shellac-an ancient natural material
Shellac is known for more than 3000 years
e-

## Slide 63
Shellac is soluble in ethanol
Curing temperature is ~60-80C;
No vacuum required for drying
Makes excellent drop cast and spin coated films
Has excellent dielectric properties (used in electrical insulation)
Possible usage as encapsulate
e-
Notes: 63

## Slide 64
Ecoflex® BASF
Hard Gelatine Capsule
Caramelized Sugar
e-

## Slide 65
Lactose / C60 OFET on Glass
W = 1 mm; L = 100 µm
Glucose / C60 OFET on Glass
µ = 0.085 cm2/Vs
C0d = 2.15 nF/cm2
µ = 0.055 cm2/Vs
C0d = 6.8 nF/cm2
Negligible hysteresis in OFETs
Solution processed natural dielectrics are good insulators
e-

## Slide 66: Exotic Materials for Bio-Organic Electronics
e-

## Slide 67: Indigo (“The color of Pharaos”) is a material known since antiquity (~4000 years) and is currently the most industrially mass-produced pigment
Indigofera suffruticosa
Indigo-dyed denim fabric
20 million killograms produced annually (~3$/kg)
e-

## Slide 68: Indigo shows promising semiconducting properties
Thermally and photochemically stable molecule with a sublimation temperature of 185 oC.
Minimal intramolecular π-conjugation
e-

## Slide 69
π-conjugated molecules exist in nature : candidates for organic electronics ?

## Slide 70: Hydrogen bonding – from water to DNA and RNA

## Slide 71: Hydrogen bonding – cellulose and kevlar
Kevlar para-aramid fibers
cellulose

## Slide 72
indigo
dihydroxyanthroquinone
Historical dyes of natural origin nearly all feature hydrogen bonding
Classics in Spectroscopy, S. Berger,
D. Sicker, Wiley-VCH (2009)

## Slide 73
Indigo and alizarin are responsible for the blue and red of many national flags

## Slide 74
Hydrogen-bonded chromophores are ubiquitous in dyeing art/science

## Slide 75: Indigo is produced by several species of plants
Oxidative dimerization
Woad leaves

## Slide 76: Indigo shows reversible 2e- oxidation and reduction electrochemistry

## Slide 77: Indigo adopts a highly crystalline morphology on many substrates
Indigo [100] plane prominently developed in growth direction

## Slide 78: Tyrian Purple dye (6,6’-dibomroindigo) was the most prized pigment in antiquity
Bolinus Brandaris
(Muricidae and Thaisidae families)
East-Roman (Byzanz) Emperor Justinian

## Slide 79
Tyrian Purple, like Indigo, is highly crystalline and shows the same electrochemistry

## Slide 80: Improved mobility could be explained by tighter π-stacking of tyrian purple relative to indigo
π-π 4.85 Å
π-π 5.77 Å
indigo
Tyrian purple

## Slide 81: Structure-packing-transport relationship
Material | Space group | π-π intermolecular distance
Indigo | P21/c | 5.77
6,6’-difluoro | P21/c | 6.04
6,6’-dichloro | P-1 | 3.75
6,6’-dibromo | P21/a | 4.85
6,6’-dimethyl | P21/c | 4.81
6,6’-dimethoxy | P21/c | 6.25
5,5’,6,6’-tetramethoxy | P42/n | none
5,5’-dichloro | P21/c | 4.54
4,4’-dichloro | P21/n | 6.53
4,4’-dibromo | P21/n | 7.46

## Slide 82: Quinacridone is the H-bonding cousin of Pentacene
Indigo
Quinacridone
pentacene

## Slide 83: Electrochemistry of quinacridone is the same as that of the indigoids

## Slide 84
Same peak on PEDOT, glass, and TTC

## Slide 85
We evaluated nature-inspired materials in field-effect transistors and in diodes
Aluminum
Semiconductor
PEDOT:PSS
glass|ITO
S (Au)
D (Au)
G (Al)
Al2O3
semiconductor
substrate
Organic-field effect transistor
Organic metal-semiconductor-metal diode

## Slide 86
We demonstrated fully ‚natural‘ indigo-based transistors and circuits
Advanced Materials, 24, 375-380 (2012)
me= 1 × 10-2
mh= 1 × 10-2

## Slide 87
Tyrian Purple shows significantly higher mobility and also air stability for both electron and hole transport
AIP Advances, 1, 42132-42137 (2011)
Organic Electronics, 13, 919–924 (2012)

## Slide 88
Tyrian Purple voltage inverters showed some of the best performance reported
Gain : 200-290

## Slide 89: Indigoids show strong island formation and distinct crystallites of several hundred nanometers size
80 nm of Indigo on Al2O3/TTC
80 nm of Tyrian Purple on Al2O3/TTC
Crystallites = 200-600 nm , channel length = 80 mm !

## Slide 90: Tyrian Purple demonstrates exceptional stability in air
Al | p-Si | Tyrian Purple (80 nm) | Al

## Slide 91
‘Intermolecular hydrogen-bonded organic semiconductors – quinacridone versus pentacene’
E.D. Głowacki,L. Leonat, M. Irimia-Vladu, APL 2012

## Slide 92
e-
Hydrogen Bonded Analogues of Pentacene/Tetracene
Air Stable Operation of OFETs is Possible !

## Slide 93: Conclusions
indigo and its derivatives are natural-origin materials performing as state-of-the-art ambipolar semiconductors
high-performance devices based on natural dyes operate stably in air
hydrogen-bonded indigoids could be a synthetic building block for novel organic semiconductors
NOW WE CAN BEAT THE STABILITY CRITERIA !

## Slide 94
What is the next challenge in
Organic Solar Energy Conversion?
Solar energy into chemical energy
e-

## Slide 95
Storage-Transport Problem
e-
Space
Time
Energy
Conversion
Consumption
later
Consumption
Somewhere else
Consumption
later and somewhere else
Storage of Energy
Transport
Energy
Transportable fuel created by solar energy conversion !!!

## Slide 96
Interfacing two R&D worlds
CO2 EMISSIONS
CLIMATE CHANGES
RENEWABLE
ENERGIES
RECYCLE CO2 !!!
CREATE FUEL
INTERFACE BETWEEN CO2 REDUCTION AND
RENEWABLE ENERGY CREATION
Future recycling of CO2 as important mission of renewable energies
e-

## Slide 97
Natural Photosynthesis
e-

## Slide 98: Recycling of CO2
Over 90 % of emitted CO2 is generated by energy products.
To convert back CO2 to fuels hydrogen or energy is required.
One promising field in this direction is the photochemical, electrochemical or biochemical reduction of carbon dioxide
e-

## Slide 99
IS IT POSSIBLE TO RECYCLE CO2?
The answer is yes!
e-

## Slide 100
e-

## Slide 101
RECYCLING CO2
e-
Methanol as carrier and storage of energy
a.) Methanol can be mixed to gasoline
b.) Methanol is used in fuel cells
c.) Methanol is starting chemical for
Many other derivatives
George Olah, Nobel Prize 1994
Univ. of Southern California, USA

## Slide 102
Inverse Fuel Cells
e-

## Slide 103
Indirect CO2 Reduction – A Known Technology
e-

## Slide 104
Direct CO2 Reduction – A More Elegant Way
Solar/Electric Energy
Catalyst as Redox
Mediator for
Direct CO2 Reduction
CO2 / H2O
Solar Fuel
e-

## Slide 105
http://www.solar-fuel.net/
e-

## Slide 106
Breites nicht regelbares
Schwankungspektrum stellt
unlösbare Anforderung an
Netzbetrieb
Strombeitrag kann daher
nur kleinen Teil des
Bedarfs decken
Chart: Windeinspeisung E.ON Transpower Netz Juni 2009
Schwankung zwischen 0% und 100%
Wind Deutschland: Durchschnitt 18%
PV Deutschland: Durchschnitt 10%
MW
Kaltfront 3.6.09:
~ 4 GW x 20 h = 80 Millionen kWh
These 2
e-

## Slide 107
Seasonal Fluctuations In Photovoltaics:
e-
Notes: 107

## Slide 108
Moved to Stuttgart, Germany 2010
Demonstration of Prototype October 2009
Demonstration of 20 MW 2012-2013
Change the name to ETOGAS
Audi Collaboration 2011-
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 109
The Solar Fuel Prototype
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 110
Development & Demonstration Plant
10 kW electrical input
Product: methane (up to 20 m³ / day)
Completion: November 2009
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 111
prototype container side view
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 112
prototype container back entrance
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 113
absorber unit
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 114
water electrolyzer
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 115
electrodialysis stack
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 116
CH4 storage and fuel maker
Designed and fabricated in ZSW Stuttgart, Germany
e-

## Slide 117
e-
Courtesy of Dr. Pengg, Audi Corp.

## Slide 118
e-
Courtesy of Dr. Pengg, Audi Corp.

## Slide 119
e-
Courtesy of Michele Aresta, Univ. of Bari, Italy

## Slide 120
e-

## Slide 121
CO
2
e-, H+
H2
O O
O O
D
A
B
C
NH2
HO
COONa
/K
ONa
/K
O
C
H2N NH2
O
O O
O
O O
O
n
+
N
RC
º
CR
RNH2
+ R’X
O2
ROH
O
C
RO OR
O O
O
O
O
R
R
RNHC
O
OR’
COOR
CO
COOH
COOH
H2C=CH2
COOH
HOOC
C
OH
O
Br
COOH
HOOC
COOH
+
RNH2
CnH2n+2
CnH2n
H3COH
HCONHR
HCOOH
CO2
n
n
e-
Courtesy of Michele Aresta, Univ. of Bari, Italy

## Slide 122: The CO2 Technological Utilization 18 Mt/y
Additive to beverages
Food packing/conservation
Cereals preservation (bactericide)
Fire estinguisher
Water treatment
Mechanicl industry (moulding,…)
Dry-washing
Air-conditioning
Extraction (scf and EOR)
Courtesy of Michele Aresta, Univ. of Bari, Italy
e-

## Slide 123
Photocatalytic reduction of carbon dioxide using a
SACRIFICIAL AGENT……..
D = sacrificial organic electron donor
P = photosensitizer
Value of CO vs value of the sacrificial organic molecule
D
D+
P*
P-
P
MRed
MOx
CO2
CO
hv
e-

## Slide 124
Photoinduced Charge Generation
e-
LUMO
HOMO
Red
Ox
Red
Ox
Photoinduced Redox Chemistry

## Slide 125
e-
Courtesy of Michele Aresta, Univ. of Bari, Italy

## Slide 126
e-
Bulk Heterojunction Electrodes
in Photoelectrochemical CO2 Recycling

## Slide 127
e-
Courtesy of Tsukasa Yoshida, Yonezawa, Japan

## Slide 128
e-
Courtesy of Tsukasa Yoshida, Yonezawa, Japan

## Slide 129
e-
Courtesy of Tsukasa Yoshida, Yonezawa, Japan

## Slide 130
e-
Courtesy of Tsukasa Yoshida, Yonezawa, Japan

## Slide 131
e-
Courtesy of Tsukasa Yoshida, Yonezawa, Japan

## Slide 132
Photochemical Reduction of CO2
K. Oppelt, D. Egbe, U. Monkowius, M. List, M. Zabel, N.S. Sariciftci, G. Knör Journal of Organometallic Chemistry 696 (2011), 2252
Homogeneous photocatalysts as well as electrocatalyst,
Oppelt, Portenkirchner 2011
e-

## Slide 133
e-
Engelbert Portenkirchner et al, Minireview

## Slide 134
e-

## Slide 135
e-

## Slide 136
e-

## Slide 137
From
CO
2
and H
2
O
to
CH
3
OH at
rt
•
CO
2
aq
à
HCOO
-
Formate
dehydrogenase
•
HCOO
-
à
H
2
CO
Formaldehydedehydrogenase
•
H
2
CO
à
CH
3
OH
Methanoldehydrogenase
•
NAD
+
/NADH
is
the
source
of
energy
.
•
Key issue
:
how to reverse
the NAD
+
/NADH
couple
after
oxidation
?
•
Use
of chemical systems for solar light harvesting
and conversion
or
r
Coupling Chemistry and Biotechnology:
e-

## Slide 138
Scheme of the enzymatic reduction of CO2
Reaction conditions
Solution buffered at pH 7
T = 37 °C
P = 1 atm
e-

## Slide 139
e-

## Slide 140
1.6 mL TEOS
4 mL of solution of
Sodium Alginate 2% (m/v)
In deionized water
1 mL solution
FatoDH (10.0 mg)
FideDH (10.0 mg)
ADH (10.0 mg)
In buffer TRIS-HCl 0.1 M (pH 7)
Drop by drop addition in
20 mL CaCl2 0.2 M+TESO
Sol-gel-formation time 30 min
Filtration
Washing with water
e-
Michele Aresta, Bari, Italy

## Slide 141
e-
Stefanie Schlager et al; 2013

## Slide 142
Interdisciplinary R & D
Photochemistry
Photophysics
Photocatalysis
Biocatalysis
Electrocatalysis
Prototyping
testing
System
Integration
Engineering
Recycling CO2
e-

## Slide 143
LIOS
Linz Institute for Organic Solar Cells
Physics of Organic Semiconductors:
1.) Photoexcited spectroscopy
2.) Photoconductivity
3.) Thin film characterization
4.) Nanoscale engineering
5.) Nanoscale microscopy (AFM, STM...)
6.) In situ spectro-electrochemistry
Organic/Hybrid
Solar Cells
CO2 Recycling into
Synthetic Fuels
Spectroscopy
and
Electrochemistry
„Incubator“ for small high tech spin-off companies
Bio-Organic
Electronic Devices
e-

## Slide 144
Acknowledgements
Members of LIOS:
Helmut Neugebauer, Markus Scharber, Mathew White, Mihai Irimia-Vladu, Philipp Stadler, Jacek Gasiorovski, Daniel Egbe, Stefanie Schlager, Engelbert Portenkirchner, Eric Glowacki, Lucia Leonat, Marek Havlicek, Patrick Denk, Gerda Kalab, Christine Hinterberger, Dogukan Apaydin, Katheryna Gutnichenko, Elisa Tordin, Christine and Sandra Enengl, Halime Coskun, Zeynep Bozkurt, Daniela Hiemetsberger, Cigdem Yumusak, Lukas Bernhauser, Melanie Weichselbaumer and
many long term visitors …
Uni. Linz, Collaborators.: Siegfried Bauer, Martin Kaltenbrunner, Helmut Sitter, G. Knoer, Uwe Monkowius, Kerstin Oppelt, Achim Hassel,
Thomas Klar, Wolfgang Heiss…
Funded by:
Austrian Foundation for Advancement of Science (FWF) Wittgenstein Prize, Indigo Project
FFG Projects,
e-

## Slide 145
Sign our petition at www.solar4peace.org
e-

## Slide 146
sign our petition
e-

## Slide 147
sign our petition
e-

## Slide 148
sign our petition
e-

## Slide 149
Future is…
Convergence of multiple crisis conditions:
1.) Energy crisis (oil running out)
2.) Climate crisis (CO2 and global warming)
3.) Demographic crisis (10 Billion population)
4.) Economic crisis (see your daily newspapers)
Will converge to a difficult future around 2050
WE NEED A
SOLAR-MARSHALL-PLAN
e-

## Slide 150
THANK YOU FOR YOUR ATTENTION